Copyright Information of the Article Published Online

| TITLE | Electron probe microanalysis оf experimentally stimulated osteoarthrosis in dogs |
| --- | --- |
| AUTHOR(s) | Tatyana Stupina, Michael Shchudlo, Michael Stepanov |
| CITATION | Stupina T, Shchudlo M, Stepanov M. Electron probe microanalysis оf experimentally stimulated osteoarthrosis in dogs. World J Orthop 2017; 8(9): 681-687 |
| URL | http://www.wjgnet.com/2218-5836/full/v8/i9/681.htm |
| DOI | http://dx.doi.org/10.5312/wjo.v8.i9.681 |
| OPEN ACCESS | This article is an open-access article which was selected by an in-house editor and fully peer-reviewed by external reviewers. It is distributed in accordance with the Creative Commons Attribution Non Commercial (CC BY-NC 4.0) license, which permits others to distribute, remix, adapt, build upon this work non-commercially, and license their derivative works on different terms, provided the original work is properly cited and the use is non-commercial. See: http://creativecommons.org/licenses/by-nc/4.0/ |
| CORE TIP | In this basic study we present the development of methods of articular cartilage preparation for X-ray-electron probe microanalysis and elements content in articular cartilage in animal experimentally induced (IOA) osteoarthrosis and during spontaneous animal aging (SA). SA was characterized by calcium and phosphorus storage in deep and calcified articular cartilage zones and compensatory increase of sulfated glycosaminoglycans in intermediate and deep zones. In IOA more intensive storage of calcium but few phosphorus in intermediate zone were marked. As for Sulphur content, all zones of uncalcified cartilage in two-year-old animals with IOA were comparable with cartilage of five-year-old intact animals. |
| KEY WORDS | Osteoarthrosis; Articular cartilage; Dog; X-ray electron probe microanalysis |
| COPYRIGHT | © The Author(s) 2017. Published by Baishideng Publishing Group Inc. All rights reserved. |
| NAME OF JOURNAL | World Journal of Orthopedics |
| ISSN | 2218-5836 |
| PUBLISHER | Baishideng Publishing Group Inc, 7901 Stoneridge Drive, Suite 501, Pleasanton, CA 94588, USA |
| WEBSITE | Http://www.wjgnet.com |

Basic Study

Electron probe microanalysis оf experimentally stimulated osteoarthrosis in dogs

Tatyana Stupina, Michael Shchudlo, Michael Stepanov

Tatyana Stupina, Michael Shchudlo, Michael Stepanov, Laboratory of Morphology, FSBI Russian Ilizarov Scientific Center “Restorative Traumatology and Orthopaedics”, 640014 Kurgan, Russia

Author contributions: Stupina T, Shchudlo M and Stepanov M substantially contributed to the conception and design of the study, acquisition, analysis and interpretation of data; all authors drafted the article and made critical revisions related to the intellectual content of the manuscript, and approved the final version of the article to be published.

Correspondence to: Dr. Tatyana Stupina, Senior Researcher, Laboratory of Morphology, FSBI Russian Ilizarov Scientific Center “Restorative Traumatology and Orthopaedics”, M. Ulianova Street 6, 640014 Kurgan, Russia. stupinasta@mail.ru

Telephone: +7-890-58506789   Fax: +7-352-2454060

Received: January 25, 2017  Revised: May 26, 2017  Accepted: July 14, 2017

Published online: September 18, 2017

Abstract

AIM

To develop methods of articular cartilage preparation for X-ray-electron probe microanalysis and to study its elements content in experimental osteoarthrosis.

METHODS

Twenty dogs aged 2-8 years were divided in research (aged 2 years, induction of osteoarthrosis - IOA) and intact group. Intact group included three subgroups (aged 2, 5 and 8 years). Samples of cartilage after araldite saturation and pouring were partially cut into semithin sections stained with methylene blue and with methylene blue-basic fuchsin. Their smooth surfaces were investigated by X-ray-electron probe microanalysis. Spatial distribution of sulfur, calcium and phosphorus and their concentrations (weight %) were investigated.

RESULTS

X-ray electron probe microanalysis revealed non-uniform sulfur distribution in cartilage of intact animals: Its content increases from superficial zone to deep one, this regularity was preserved in animals with IOA. Differences of IOA with spontaneous chondropathy were revealed. Spontaneous aging was characterized by calcium and phosphorus storage in deep and calcified zones and compensatory increase of sulfated glycosaminoglycans in intermediate and deep cartilage zones as evidenced by the metachromatic reaction and microanalysis data. Unlike spontaneous chondropathy connected with aging in experimentally stimulated osteoarthrosis more intensive storage of calcium but minor phosphorus in intermediate zone were marked. In IOA the calcified cartilage thinning and osteoclastic resorption are apparent with few changes of elements composition; the only difference from control is minority phosphorus content.

CONCLUSION

The obtained results demonstrate specific tricks of X-ray electron probe microanalysis and its possibility in the research of mechanisms of articular cartilage alterations in osteoarthrosis.

Key words: Osteoarthrosis; Articular cartilage; Dog; X-ray electron probe microanalysis

Stupina T, Shchudlo M, Stepanov M. Electron probe microanalysis оf experimentally stimulated osteoarthrosis in dogs. World J Orthop 2017; 8(9): 681-687  Available from: URL: http://www.wjgnet.com/2218-5836/full/v8/i9/681.htm  DOI: http://dx.doi.org/10.5312/wjo.v8.i9.681

Core tip: In this basic study we present the development of methods of articular cartilage preparation for X-ray-electron probe microanalysis and elements content in articular cartilage in animal experimentally induced (IOA) osteoarthrosis and during spontaneous animal aging (SA). SA was characterized by calcium and phosphorus storage in deep and calcified articular cartilage zones and compensatory increase of sulfated glycosaminoglycans in intermediate and deep zones. In IOA more intensive storage of calcium but few phosphorus in intermediate zone were marked. As for Sulphur content, all zones of uncalcified cartilage in two-year-old animals with IOA were comparable with cartilage of five-year-old intact animals.

INTRODUCTION

Osteoarthrosis (OA) has great social impact in terms of disability, pain, illness and treatment costs. Pathogenesis of OA involves the structures of the whole joint especially subchondral bone and synovium but is characterized predominantly by articular cartilage destruction[1]. Cartilaginous tissues possess relatively few amounts cells (chondrocytes) that account 1%-5% of volume[2] and large amounts of extracellular matrix that constitutes the bulk of tissue and protects chondrocytes from mechanical overloading.

Cartilage destruction in osteoarthrosis is multifactorial cascade process in which participate both cells and extracellular matrix, especially sulfated glycosaminoglycans. These last are included in proteoglycans and play the leading role in support of tissue homeostasis, architectonics and mechanical stability, cellular mitogenic activity, receptive functions and intercellular relations[3].

Mineralization of cartilage has been associated with OA progression and cartilage destruction[4] but some authors consider it as primarily an effect of aging[5].

A lot of biochemical and microscopical methods are used in modern researches of cartilage content and structure but x-ray-microprobe analysis was performed very rare though it permit to evaluate glycosaminoglicans and mineral content by corresponding chemical elements.

To develop the optimal methods of articular hyaline cartilage sample preparation for X-ray-electron probe microanalysis and to compare its elements content in intact animals and in animals with experimentally induced osteoarthrosis.

MATERIALS AND METHODS

Twenty healthy adult mongrel dogs of either sex, aged 2-8 years, weighing 18-25 kg, were used in this study. All animals have received human care in compliance with the protocol approved by the Institutional Ethical Committee. The animals were acclimatized to laboratory conditions for one month prior experimentation. Dogs were housed in individual cages (floor area 4.5 m2) and were provided water three times daily and food two times daily with a measured volume. Animals were divided in research (aged 2 years) and intact group (control). Intact group included three subgroups (aged 2, 5 and 8 years). In research group modelling of primary gonarthrosis was performed by reduction of limb blood supply and knee immobilization[6]. So, dogs of research group were operated. Anesthesia was first induced with intramuscular injections of atropine, dimedrol and xylazine and then maintained with intravenous injection sodium pentobarbital (30 mg/kg i.v.). Briefly, each femoral artery was freed from surrounding tissues and after proximal and distal ligation was resected. Each knee joint were immobilized with external fixation apparatus. After 28 d of immobilization dogs of research group were euthanized. Dogs of intact group were also euthanized by barbiturate overdose (intravenous injection, 150 mg/kg pentobarbital sodium) for tissue collection.

Samples of cartilage were harvested from lateral femoral condyles - presented in Figure 1A. Samples consisted of slices 2-3 mm thick, 5-6 mm long and 2-3 mm wide were cut with a scalpel tangentially within articular cartilage - presented in Figure 1B. Samples were fixed in glutaraldehyde-paraformaldehyde mixture excluding postfixation in tetraoxide osmium because X-ray peaks of heavy metals may mask and overlap on rays of analyzed elements[7,8]. Taking into consideration very high water content in cartilage[2] the specimens were dehydrated with smooth transition from ethanol to aceton according to known methods[9] but with increasing of exposition in 70%-96% ethanol to within the hour. Stages of araldite saturation and pouring were performed according to recently described method[10]. Increased density of cartilage matrix in araldite in comparison with native material decrease volume of X-ray excitation and provide the increase of microanalysis sensitivity.

Further investigation included two stages. At the first stage epoxy blocks were partially cut into semithin (1 mkm) sections with a glass knife using ultramicrotome “Nova” (LKB, Sweden). Slices were stained with methylene blue (metachromatic reaction for sulfated glycosaminoglycans) and with methylene blue-basic fuchsin (for detection of matrix basophily). Histology slides were examined using the “Opton-3” photomicroscope (Germany).

At the second stage smooth surfaces of epoxy blocks resulting from semithin slices cutting were investigated by x-ray-electron probe microanalysis. This technique prevents artifacts and saves the sample preparation time excluding the stage of grinding and polishing.

Three blocks was selected randomly from each animal. They were attached to polished clean aluminium discs with current-conducting adhesive. Surfaces of epoxy blocks were exposed to silver deposition using Eico IB-6 ion coater and JEOL JEE-4X vacuum evaporator. The investigation of element composition was performed using scanning electron microscope JSM-840 (JEOL, Japan) equipped with energy dispersive X-ray analyser (INCA 200, Oxford Instruments).

Results were obtained as smart maps, showing spatial distribution of elements and quantitative data in weight per cents. Spatial distribution of sulfur, calcium and phosphorus and their concentrations (S, Са, P - weight %) were investigated. For standard results equipment was calibrated by comparison templet made of wollastonite (СаО: SiO2). Two regimens were used for collecting X-ray spectra: Scanning line and scanning area - presented in Figure 2. In the second regimen strict longitudinal alignment of parallel scanning rows without overlapping fields provided the most representative total sample.

Statistical analysis

For quantitative data analysis the unpaired Student t test and Mann-Whitney U test were used (software package Attestat Program, version 9.3.1, developed by I.P. Gaidyshev, Certificate of Rospatent official registration No. 2002611109). If the P-value was less than 0.05, the data was considered statistically significant.

RESULTS

In 2 years-aged intact group metachromatic reaction in interterritorial matrix of superficial zone was moderate but in territorial matrix of intermediate and deep zones it was highly intensive - presented in Figure 3A. X-ray electron probe microanalysis revealed nonuniformity of Sulphur zonal distribution - presented in Figure 3B.

In IOA (induced osteoarthrosis) group metachromatic reaction was localized, its intensity was lowered and accompanied with fibrillation of matrix in superficial zone. Intensively basophilic matrix was revealed in intermediate and deep zones and presented in Figure 4A and B. The calcified cartilage zone was thinned or absolutely absent in some areas (Figures 4A and 5). At the borderline between calcified cartilage and subchondral bone the osteoclastic resorption was marked - presented in Figure 4C.

In 5 years-aged intact group histochemical reaction for sulfated glycosaminoglycans was weak, metachromasy was focal (Figure 6A), matrix of superficial zone was basophilic, many of cells had signs of destruction.

In 8 years-aged intact group metachromatic reaction was also focal, locuses of intensive metachromasy were revealed in intermediate and deep zones (Figure 6B), cartilaginous cells had increased sizes, light homogeneous nuclei and basophilic cytoplasm. Territorial matrix of deep zone was basophilic.

In IOA group S were decreased in all of cartilage zones besides calcified, but its distribution with maximal meanings in intermediate and deep zones was the same as in two-year-old intact group. In five-year-old intact group in comparison with two-year-old intact group S was decreased in superficial, intermediate and deep zones, but increased in calcified cartilage. In eight-year-old intact group in comparison with two-year-old intact group S was increased in intermediate, deep and calcified cartilage zones, but not in superficial zone - presented in Table 1.

In IOA group in comparison with two-year-old intact group Ca was increased in all zones of cartilage besides the calcified. In five-year-old intact group Ca was increased only in superficial zone and in calcified cartilage. In eight-year-old intact group more expressed increase in deep and calcified zones were marked (Table 1).

Changes of P were differently directed. In IOA it was increased in intermediate and deep zones but decreased in calcified cartilage. In 5 years-aged and especially in 8 years-aged intact groups P was increased in all zones including calcified cartilage - presented in Figure 7 and Table 1.

DISCUSSION

So, X-ray electron probe microanalysis revealed non-uniform serum distribution in cartilage of intact animals: its content increases from superficial to deep zone, this regularity was preserved in animals with induced experimental osteoarthrosis. The obtained data are in agreement with literature: The aggrecan content in superficial zone is lower than in others[11]. It is known that metabolism of sulfated glycosaminoglycans changes in the early stages of articular cartilage damage[12].

Recently we obtained histological characteristics of articular cartilage in experimentally induced osteoarthrosis[13,14] corresponding to grade 1-3 according to OARSI classification[15]. It was revealed[14] that in this experimental model chondrocytes of intermediate zone were the most vulnerable: More than 50% cells had signs of necrosis or apoptosis. It is known that apoptotic bodies contain alkaline phosphatase and precipitate calcium promoting cartilage calcification[16].

According to other authors hypertrophic chondrocytes of osteoarthrotic cartilage produce large amounts of collagen X, matrix proteinase 12 and alkaline phosphatase influencing calcification[17]. Ohira and Ishikawa[18] (1986) found precipitates of hydroxiapatite crystals around degenerated chondrocytes.

In current research substantial difference of experimentally induced osteoarthrosis from spontaneous chondropathy were revealed. Spontaneous aging characterizes by calcium and phosphorus storage in deep and calcified zones and compensatory increase of sulfated glycosaminoglycans in intermediate and deep cartilage zones as evidenced by the metachromatic reaction and microanalysis data. Unlike spontaneous chondropathy connected with aging in experimentally reduced osteoarthrosis more intensive storage of calcium but minor phosphorus in intermediate zone were marked. The revealed contradistinction is in agreement with research of human aging, which leads to suggest that phosphorus exuded from bones storages in arteries and cartilage tissue[19].

In experimentally induced osteoarthrosis the calcified cartilage thinning and osteoclastic resorption are apparent with few changes of elements composition; the only difference from control is minority phosphorus content.

Preparation of biologic samples for X-ray electron probe microanalysis perform according the same principles as preparation for electron microscopy but possess its own specific tricks; peculiar properties of research object also must be taken into consideration. The obtained results demonstrate definitely the possibility of X-ray electron probe microanalysis in the research of mechanisms of articular cartilage alteration in osteoarthrosis, these changes is documented and assessed quantitatively.

ACKOWLEDGMENTS

The authors would like to thank the members of the engineering group for their technical support and I.P. Gaidyshev for his help in statistical analysis.

COMMENTS

Background

Multiple biochemical and microscopic methods are used in modern researches of cartilage content and structure in normal and diseased human and animal beings but x-ray-microprobe analysis was performed very rare though it permit to evaluate glycosaminoglicans and mineral content by corresponding chemical elements. The optimal methods of articular hyaline cartilage sample preparation for x-ray-electron probe microanalysis and comparison of its elements content in intact animals of different ages and in animals with experimentally induced osteoarthrosis were not investigated.

Research frontiers

Previous research have already proved that in this experimental model of primary osteoarthrosis chondrocytes of intermediate zone were the most vulnerable and that apoptotic bodies promote cartilage calcification.

Innovations and breakthroughs

This is the first study evaluating substantial difference of experimental gonarthrosis induced by reduction of limb blood supply and knee immobilization from spontaneous age-related chondropathy. The optimized methods of articular hyaline cartilage sample preparation for x-ray-electron probe microanalysis are described.

Applications

In experimentally induced osteoarthrosis the uncalcified cartilage was characterized with minority Sulphur content, calcium and phosphorus storage in comparison with intact animals of corresponding age. The calcified cartilage thinning and osteoclastic resorption in induction of osteoarthrosis are apparent with few changes of elements composition; the only difference from control is minority phosphorus content.

Terminology

Experimentally stimulated osteoarthrosis in used biological model histologically corresponds to grade 1-3 according to OARSI classification.

Peer-review

Stupina et al developed methods of articular cartilage preparation for X-ray-electron probe microanalysis and to study its elements content in experimental osteoarthrosis. It is well designed and written manuscript. It is a potential important study to the fields of osteoarthrosis research, diagnosis and therapy.

REFERENCES

1	Hunter DJ, Felson DT. Osteoarthritis. BMJ 2006; 332: 639-642 [PMID: 16543327 DOI: 10.1136/bmj.332.7542.639]

2	Jerosch J. Effects of Glucosamine and Chondroitin Sulfate on Cartilage Metabolism in OA: Outlook on Other Nutrient Partners Especially Omega-3 Fatty Acids. Int J Rheumatol 2011; 2011: 969012 [PMID: 21826146 DOI: 10.1155/2011/969012]

3	Seidman AM, Korel AV. Structural and functional features of the plate human vertebral body growth during critical periods of growth. Surg Vertebral 2004; 2: 113-120

4	Fuerst M, Bertrand J, Lammers L, Dreier R, Echtermeyer F, Nitschke Y, Rutsch F, Schäfer FK, Niggemeyer O, Steinhagen J, Lohmann CH, Pap T, Rüther W. Calcification of articular cartilage in human osteoarthritis. Arthritis Rheum 2009; 60: 2694-2703 [PMID: 19714647 DOI: 10.1002/art.24774]

5	Mitsuyama H, Healey RM, Terkeltaub RA, Coutts RD, Amiel D. Calcification of human articular knee cartilage is primarily an effect of aging rather than osteoarthritis. Osteoarthritis Cartilage 2007; 15: 559-565 [PMID: 17276093 DOI: 10.1016/j.joca.2006.10.017]

6	Makushin VD, Stepanov MA, Stupina TA, Inventors. Method of Simulating Osteoarthrosis of Knee. Russia patent RF 2452999. 2012. Iun 10

7	Goldstein J, Newbury D, Echlin P, Dzhoy D, Fiori C, Lifshin E. Raster electronic microscopy and x-rayed Microprobe Analysis. М: World 1984: 1: 348

8	Shahlamov VA, Buravkov SV. Application of X-ray local microanalysis in biology and medicine. Arkh Anat Histol Embriol 1983; 4: 95-107

9	Weakley B. A beginners handbook in biological electron microscopy. М: World 1975: 324

10	Stupina TA, Shchudlo MM. A method for making preparations from nondecalcified articular cartilage with sublying subchondral bone for multipurpose studies. Bull Exp Biol Med 2014; 157: 388-390 [DOI: 10.1007/s10517-014-2576-z]

11	Anderson HC, Hodges PT, Aguilera XM, Missana L, Moylan PE. Bone morphogenetic protein (BMP) localization in developing human and rat growth plate, metaphysis, epiphysis, and articular cartilage. J Histochem Cytochem 2000; 48: 1493-1502 [PMID: 11036092]

12	Pavlova VN, Pavlov GG, Shostak NA, Slutsky LI. Joint: The morphology, clinic, diagnostics, treatment. M: OOO “Publisher” Medical News Agency”, 2011: 552

13	Stupina TA, Shchudlo NA, Stepanov MA. Structural reorganization of the main joint components during the experimental modeling of osteoarthrosis with reduced blood supply. Morfologiia 2014; 146: 61-65

14	Shevtsov VI, Makushin VD, Stepanov MA, Stupina TA. The problem of the knee osteoarthrosis modeling in dogs for the purpose of pathogenesis studying (experimental morphological study). Genius Orthop 2012; 1: 38-42

15	Pritzker KP, Gay S, Jimenez SA, Ostergaard K, Pelletier JP, Revell PA, Salter D, van den Berg WB. Osteoarthritis cartilage histopathology: grading and staging. Osteoarthritis Cartilage 2006; 14: 13-29 [PMID: 16242352 DOI: 10.1016/j.joca.2005.07.014]

16	Adams CS, Shapiro IM. The fate of the terminally differentiated chondrocyte: evidence for microenvironmental regulation of chondrocyte apoptosis. Crit Rev Oral Biol Med 2002; 13: 465-473 [PMID: 12499240]

17	Tchetina EV. The mechanisms of embryogenesis in osteoarthritis: the role of differentiation of chondrocytes in articular cartilage resorption. Sci Practical Rheumatol 2010; 3: 65-77

18	Ohira T, Ishikawa K. Hydroxyapatite deposition in articular cartilage by intra-articular injections of methylprednisolone. A histological, ultrastructural, and x-ray-microprobe analysis in rabbits. J Bone Joint Surg Am 1986; 68: 509-520 [PMID: 3007526]

19	Tohno Y, Tohno S, Minami T, Moriwake Y, Utsumi M, Yamada M. A possible balance of phosphorus accumulations among bone, cartilage, artery, and vein in single human individuals. Biol Trace Elem Res1999; 69: 241-248 [PMID: 10468161 DOI: 10.1007/BF02783876]

FIGURE LEGENDS

Figure 1  Condyles of canine thigh bone after experimental modelling of osteoarthrosis (A), scheme of articular cartilage harvesting (B).

Figure 2  X-ray electron probe microanalysis of articular cartilage in intact dog. A: SEM micrograph of articular cartilage and subchondral zone; B:  Scanning line regimen, graph shows calcium distribution on line; C: Scanning area regimen shows calcium distribution on the sample surface. Instrumental magnification × 110.

Figure 3  Articular cartilage of intact dog. A: Semithin section, methylene blue stain. Ob. -6.3 х; oc. -12.5 х; B: Smart map shows sulphur distribution on scanned line. Instrumental magnification 170.

Figure 4  Articular cartilage in dog with experimentally induced osteoarthrosis. Methylene blue - basic fuchsin staining. A: General appearance. Ob. - 6.3 x, oc. - 12.5 x; B: Focal basophilia of intercellular matrix in deep zone. Ob. - 100 OI, oc. - 12.5 x; C: Osteoclast, resorbing the ground substance of calcified cartilage. Howship lacuna (arrow). Ob. - 100 OI, oc. - 12.5 x.

Figure 5  X-ray electron probe microanalysis of articular cartilage in dog with experimentally induced osteoarthrosis. A: SEM micrograph of articular cartilage and subchondral zone; B: Scanning line regimen, graph shows calcium distribution on line; C: Scanning area regimen shows calcium distribution on the sample surface. Instrumental magnification 100.

Figure 6  Age-related changes of articular cartilage in intact group. Semithin section.  Methylene blue - basic fuchsin staining. A: Focal metachromasy of articular cartilage in five year old dog. Ob. -6,3 х; oc. - 12,5 х; B: Intensive metachromasy in intermediate and deep zones of articular cartilage in eight year old dog. Ob. -16 х; oc. - 12,5 х.

Figure 7  X-ray electron probe microanalysis of articular cartilage in intact five years old dog. A: SEM micrograph of articular cartilage and subchondral zone; B: Scanning line regimen, graph shows phosphorus distribution on line; C: Scanning area regimen shows phosphorus distribution on the sample surface. Instrumental magnification 120.

FOOTNOTES

Supported by The RF Ministry of Health within government-mandated program for FSBI Russian Ilizarov Scientific Center “Restorative Traumatology and Orthopaedics” (RISC “RTO”) for Scientific Research, No. 01201155770.

Institutional review board statement: The article was reviewed by RISC “RTO” Review Board and statement including: (1) the manuscript is not simultaneously being considered by other journals or already published elsewhere; (2) the manuscript has no redundant publication, plagiarism, or data fabrication or falsification; (3) experiments involving animal subjects were designed and performed in compliance with the relevant laws regarding the animal care and use of subjects; and (4) material contained within the manuscript is original, with all information from other sources appropriately referenced.

Institutional animal care and use committee statement: All animal studies are approved by RISC “RTO” Ethical Committee - excerpts from the minutes #4 (50) under date of December 13, 2016.

Conflict-of-interest statement: The authors declare no conflict of interest.

Data sharing statement: No additional data are available.

Open-Access: This article is an open-access article which was selected by an in-house editor and fully peer-reviewed by external reviewers. It is distributed in accordance with the Creative Commons Attribution Non Commercial (CC BY-NC 4.0) license, which permits others to distribute, remix, adapt, build upon this work non-commercially, and license their derivative works on different terms, provided the original work is properly cited and the use is non-commercial. See: http://creativecommons.org/licenses/by-nc/4.0/

Manuscript source: Invited manuscript

Peer-review started: February 2, 2017

First decision: May 23, 2017

Article in press: July 15, 2017

P- Reviewer: Zhou S    S- Editor: Kong JX    L- Editor: A    E- Editor: Lu YJ

# Text boxes

Table 1  Content of chemical elements in canine articular cartilage

| Cartilage zones/groups | Superficial zone | Intermediate zone | Deep zone | Zone of calcified cartilage |
| --- | --- | --- | --- | --- |
| S (mean ± SD, weight%) |  |  |  |  |
| IOA in 2 yr | 0.18 ± 0.04a | 0.23 ± 0.02a | 0.28 ± 0.03a | 0.13 ± 0.02 |
| Intact |  |  |  |  |
| 2 yr (control) | 0.35 ± 0.01 | 0.42 ± 0.04 | 0.52 ± 0.02 | 0.14 ± 0.02 |
| 5 yr | 0.20 ± 0.02a | 0.28 ± 0.04a | 0.34 ± 0.02a | 0.28 ± 0.04a |
| 8 yr | 0.33 ± 0.03 | 0.52 ± 0.01a | 0.63 ± 0.04a | 0.41 ± 0.07a |
| Ca (mean ± SD, weight%) |  |  |  |  |
| IOA in 2 yr | 0.04 ± 0.02 | 0.08 ± 0.02a | 0.15 ± 0.02a | 9.72 ± 0.03 |
| Intact |  |  |  |  |
| 2 yr (control) | < 0.01 | 0.04 ± 0.01 | 0.09 ± 0.01 | 13.93 ± 0.02 |
| 5 yr | 0.04 ± 0.01 | 0.05 ± 0.03 | 0.10 ± 0.02 | 16.16 ± 1.04a |
| 8 yr | 0.03 ± 0.02 | 0.05 ± 0.03 | 0.22 ± 0.02a | 21.16 ± 3.04a |
| P (mean ± SD, weight%) |  |  |  |  |
| IOA in 2 yr | < 0.02 | 0.03 ± 0.01 | 0.08 ± 0.01 | 4.74 ± 0.02a |
| Intact |  |  |  |  |
| 2 yr (control) | < 0.01 | < 0.01 | < 0.01 | 6.89 ± 0.01 |
| 5 yr | < 0.02 | 0.07 ± 0.01a | 0.09 ± 0.02a | 7.44 ± 1.47a |
| 8 yr | 0.04 ± 0.02a | 0.09 ± 0.02a | 0.11 ± 0.02a | 9.44 ± 1.29a |

aP < 0.05, vs control.