Name of Journal: World Journal of Gastroenterology

Manuscript NO: 35315

Manuscript Type: ORIGINAL ARTICLE

Basic Study

Epidermal growth factor receptor immune magnetic liposomes capturecolorectalcirculating tumorcells with high-efficiency

Kuai JH et al. EGFR liposomes for colorectal CTCs capture

Jing-Hua Kuai, Qing Wang, Ai-Jun Zhang, Jing-Yu Zhang, Zheng-Feng Chen, Kang-Kang Wu, Xiao-Zhen Hu

Jing-Hua Kuai, Qing Wang, Ai-Jun Zhang, Jing-Yu Zhang, Zheng-Feng Chen, Kang-Kang Wu, Department of gastroenterology, Qilu Hospital of Shandong University, Qingdao 266035, Shandong Province, China

Xiao-Zhen Hu, Department of General Surgery, Qilu Hospital of Shandong University, Qingdao 266035, Shandong Province, China

ORCID number: Jing-Hua Kuai (0000-0002-0529-0559); Qing Wang (0000-0001-8645-801x); Ai-Jun Zhang (0000-0002-1944-4352); Jing-Yu Zhang (0000-0002-8102-9870); Zheng-Feng Chen (0000-0002-3643-4340); Kang-Kang Wu (0000-0003-0175-0439); Xiao-Zhen Hu (0000-0002-7233-5286).

Author contributions: Kuai JH, Wang Q, Zhang AJ, Zhang JY, Chen ZF, Wu KK and Hu XZ designed research; Jinghua Kuai, Qing Wang andXiaozhen Hu performed research; Aijun Zhang, Jingyu Zhang contributed new reagents/analytic tools; Jinghua Kuai,Zhengfeng Chen and Kangkang Wu analyzed data; and Jinghua Kuai and Xiaozhen Hu wrote the paper.

Institutional review board statement: The study was reviewed and approved by the Institutional Review Board of Shandong University affiliated Qilu Hospital.

Conflict-of-interest statement: All the authors declare that there is no conflict-of-interest to disclose.

Open-Access: This article is an open-access article which was selected by an in-house editor and fully peer-reviewed by external reviewers. It is distributed in accordance with the Creative Commons Attribution Non Commercial (CC BY-NC 4.0) license, which permits others to distribute, remix, adapt, build upon this work non-commercially, and license their derivative works on different terms, provided the original work is properly cited and the use is non-commercial. See: http://creativecommons.org/licenses/by-nc/4.0/

Manuscript source: Unsolicited manuscript

Correspondence to: Xiao-zhen Hu, PhD, Chief Doctor, Department of general surgery, Qilu Hospital of Shandong University, No. 758 Hefei Road, Qingdao 266035, Shandong Province, China. hu.xz@qilu.edu.com

Telephone: +86-532-66850782

Fax: +86-532-66850532

Received: September 8, 2017

Peer-review started: September 8, 2017

First decision: September 20, 2017

Revised: November 27, 2017

Accepted: December 5, 2017

Article in press:

Published online:

Abstract

AIM

To compare the capture capacity of newly self-constructed epidermal growth factor receptor (EGFR) immune magnetic liposomes (EILs) on colorectal circulating tumor cells (CTCs) with that of epithelial cell adhesion molecule (EpCAM) immunomagnetic beads.

Methods

EILs was constructed using a two-step synthesis method and the magnetic and surface characterizations were confirmed. The capture efficiency on colorectal CTCs as well as the specificity were compared between EILs and EpCAM magnetic ball.

RESULTS

The obtained EIL shave a lipid nanoparticle structure similar to cell membrane. An improved combination with cancer cells was seen in EILs compared with the modification method of combining antibody to nano/microspheres. The combination increased as the contact time extended. Compared with EpCAM immunomagnetic beads, EILs captured more CTCs in blood of colorectal cancer patients.The captured cells showed consistency with clinical diagnosis and pathology. Mutation analysis showed same results between captured CTCs and cancer tissues.

CONCLUSION

EGFR coated with magnetic liposomes showed high efficiencyand specificity in the capture of colorectal CTCs.

Key words: Epidermal growth factor receptor; Immune magnetic liposomes; Epithelial cell adhesion molecule; Circulating tumor cells; Colorectal cancer

© The Author(s) 2017. Published by Baishideng Publishing Group Inc. All rights reserved.

Core tip: epidermal growth factor receptor immune magnetic liposomes (EILs) was constructed by two-step synthesis method. The combination ability of capturing tumor cells (CTCs) in blood of colorectal cancer patients was compared between EILs andepithelial cell adhesion molecule (EpCAM) immunomagnetic beads. We found that EILs captured more CTCs than of EpCAM immunomagnetic beads with a higher efficiency and specificity.

Kuai JH, Wang Q, Zhang AJ, Zhang JY, Chen ZF, Wu KK, Hu XZ. Epidermal growth factor receptor immune magnetic liposomes capturecolorectalcirculating tumorcells with high-efficiency. World J Gastroenterol 2017; In press

Introduction

Metastasis contributes most to cancer-related deaths in patients with solid tumors. Mounting evidence ssuggested circulating tumor cells (CTCs) which can shed from a primary tumor massat the earliest stages of malignant progression played a critical role in cancer metastasis[1-3]. As a “liquid biopsy” of the tumor, CTC provides an insight into tumor biology in a critical window where intervention could actually make a difference[4-7].

Detection and characterization of CTCs is challenging owing to their extreme scarcity in blood[8-11]. Several methods have been evolving which includes immunomagnetic separation based on capture reagent-labeled magnetic beads, microfluidics-based technologies that enhance cell-surface contacts, and microfilter devices that isolate CTCs based on size difference[9,12-14]. However, the sensitivity of aforementioned methods relies greatly on the enrichment degree of CTCs and current techniques used is far from satisfactory[15-18].

Clinically, the CellSearch® System, approved by the United States Food and Drug Administration recently, is deemed as the standard method[19,20]. Epithelial cell adhesion molecule (EpCAM) antibody is used to surround the magnetic beads in the system. However, EpCAM positive cells have been found in healthy persons[21]. Moreover, epithelial-mesenchymal transition (EMT), which is vital for metastases, could result in loss of epithelial antigens in some CTCs[22-26].

Recently, a new method in which a cell bilayer membrane structured magnetic liposome prepared directly with cancer-cell capture agents-EGFR antibody was discovered[27,28]. Studies found a significant improvement in cell-capture efficiency owing to its enhanced interactions between the deformable antibody receptor-lipid bilayer structure and nanoscale cellular surface components[29,30]. Such a high-affinity cell assay can be employed to recover cancer cells from spiked whole-blood samples, in stationary magnetic separation device by anti-EGFR magnetic nano-vesicles[31,32]. On these bases of this stationary cell-capture assay, we hypothesize thatfurther improvement of cell-capture efficiency can be achieved by increasing surface activity site of magnetic beads to tumor cells.

# MATERIALS AND METHODS

# Materials

Chitosan (M.W. 5×104) was supplied by YuhuanAoxing biochemistry (Zhejiang, China) with a deacetylation degree of above 99%.Octadecylquaternized carboxymethyl chitosan (OQCMC), hydrophobic magnetic nanoparticles (BM) and hydrophilic magnetic nanoparticles (LM) wereall prepared in our lab. All other chemicals were of reagent grade and were used as received. The study has been approved by local IRB and informed consent has been gained from recruited patients.

Preparation of EGFR immune liposomes

Modified DSPE-PEG-EGFR (1.0 mg) was weighed. 3.0 mg of DOPC, 2.0 mg of OQCMC and 6.0 mg of cholesterol (Chol) were dissolved in 5.0 mL of dichloromethane (CH2Cl2). Magnetic nano bare beads (3 mL) were also added and incubated for 10 min. A certain volume of phosphate buffer solution (PBS, pH = 7.4) was added. The echo probe was used for phacoemulsification during ice bathing. After formation of the uniform emulsion, organic phase was removed by rotary evaporation. After magnetic separation, PBS was used for washing for 3 times and IML(immune magnetic liposomes) was then obtained.

A certain quantity of IML was dispersed in PBS solution. After that, EDC was added, oscillated and incubated for 3 h. The unreacted coupling agent was removeand EGFR immune liposomes (EILs) were obtained.

Characterization of EILs

The particle size and distributionwere determined byquasielastic laser light scattering with a Malvern Zetasizer (Malvern Instruments Limited, United Kingdom) at 25 ℃. About 0.2 mL of EILs suspensions were diluted into 2.5 mL water immediately after preparation. Each experiment was repeated three times. Zeta potential was measured by using a Zetasizer (Malvern, United Kingdom). Zeta limits ranged from –150 to 150 V. The magnetic properties of EILs were determined through VSM (vibrating samples magetometer, LDJ9600-1).

EILs on recognition of colorectal cancerHT-29cells in vitro

HT-29 cells (8×104)at logarithmic phase were paved on sterilecircular cover glasses in a 24-well plate.The plate was incubated with 0.5 mL of culture medium containing 10% serum at 37 ℃ and 5% CO2 overnight. When the cell fusion degree was more than 70%, 20 μL FITC labeled EILs was added. After culture for 30 min, the liquid was discarded and the precipitation was washed by PBS for 3 times before shaken for 2 min once. After shaking, 4% paraformaldehyde was added for cell fixation for 20 min and washed 3 times again with PBS. DAPI dye liquor was added in each hole away from light to stain nuclei for 10 min and washed for 3 times with PBS; the cell membrane probe Dil was added in each hole to stain for 10 min and washed 3 times with PBS. Finally, the cover glasses were removed. The fluorescence decay sealing agents were adhered on glass slides. The distributions of the immune magnetic ball inside and outside the cell membrane were observed under laser confocal microscope.

Recognition of CTCs

A three-color immunocytochemistry method was applied to identify and enumerate CTCs from non-specifically trapped white blood cells (WBCs). The markers included PE-labeled anti-CD45 (a marker for WBCs) and FITC-labeled anti-CK19 (Cytokeratin, a protein marker for epithelial cells) as well as DAPI nuclear staining. Fluorescence microscopy was employed to quantify DAPI intensities and expression levels of CK19 and CD45 in individual cells.The combined information was utilized to delineate CTCs (DAPI+/CK+/CD45-, cell sizes > 8 µm) from WBCs (DAPI+/CK-/CD45+, sizes < 15 µm) and cellular debris (DAPI-).

Clinical application of CTC capture and identification in colorectal cancer patients

The CTC capture and identification methods were similar with CellSearch, but manually operated instead. Specifically, 7.5 mL ofwhole blood was collected and centrifuged at 1000 rpm/min for 10 min. After that, the upper-middle level liquid was transferred and equal volume of PBS was added and mixed evenly.  Then 120 μL of EILs was added and incubated at room temperature for 30 min. The mixture was blended once every 10 min and the EP tube was inserted into the magnetic separation frame and absorbed for 5 min. After that, the supernatant was removed andEP tube was taken out. The captured CTC was washed once with PBS followed by staining with 30 μL of DAPI, 30 μL of CK19-FITC and 10 μL of CD45-PE in a mixture for 15 min.The deionized water was used to wash in the magnetic separation frame for 2 times. Finally, 30 μL of deionized water was added in EP tube for re-suspending. The blending liquid was evenly coated in the center for slide. After the liquid drop was dried, the cells were photographed and counted under fluorescent microscope.

DNA extracted and Mutations analysis in CTCs

The captured cells were put into a 10 μL of PCR buffer with proteinase K at 60 ℃ for overnight. We inactivated the proteinase K at 95 ℃ for 10 min. We used agarose gel electrophoresis and sequencing to determine mutations of KRAS gene. Meanwhile, we obtained DNA and analyzed the KRAS mutations from peripheral blood of the 7 colorectal cancer patients.

Statistical analysis

Statistical analysis was carried out by Prism software (GraphPad Software, Inc., La Jolla, CA). The unpaired Student’s t-test was used to compare hydrodynamic size, diffuse efficient and zeta potential between IML and EILs. A paired Student’s t-test was used to detect differences in the number of CTC captured by EpCAM immunomagnetic beads in comparison with EILs. A P value of smaller than 0.05 was considered to be statistically significant.

# Results

# Process for preparing EILs

A two-step synthesis was used to derive EILs, which was achieved through encapsulating hydrophilic or hydrophobic magnetic nanoparticles into polymeric surfactant/cholesterol vesicles. Figure 1 illustrated the preparation procedure. The as-synthesized hydrophilic magnetic nanoparticles (LM) an be encapsulated into the aqueous core of polymeric liposomes. Furthermore, evaporation of organic solvent can transfer hydrophobic magnetic nanoparticles (BM) into the aqueous phase by an interfacial process driven by the hydrophobic van der Waals interactions between the primary alkane of the stabilizing ligand in oleic acid and the secondary alkane of the OQCMC. In addition, cholesterolcan modulate membrane fluidity, elasticity, and permeability by stabilizing the polymeric liposome system.

# Characterization of EILs

Figure 2A showed the hydrodynamic diameter of IML and EILs. The results indicated that the mean hydrodynamic size of IML was 83.1 ± 1.5 nm, whereas the diffusion coefficient was 1.3758E-14 m2/s and that the mean hydrodynamic size of EILswas 104.5 ± 1.3 nm with a diffusion coefficient of1.5870E-14 m2/s.

After encapsulating with OQCMC/Chol polymeric liposomes film, the surface zeta potential of hydrophilic Fe3O4 nanoparticles could reach +41mv. After reaction of EGFR antibody, the surface zeta potential of IMLcould reach +37mv.There was no difference in Zeta potential (Figure 2B).

# Magnetic and surface characterization of EILs

Figure 2C showed the magnetization curves of IML and EILs under room temperature. Both samples show a typical superparamagnetic behavior without any hysteresis loop. The saturation magnetization value of IML and EILs was 40 emu/g and 20 emu/gat 300 K. The volume fraction of magnetite can be further increased by increasing the number of layer of lipid coating.

Characteristics of CTCs

As shown in Figure 3A, the captured CTCs cells were DAPI+/CK+/CD45-, with cell sizes more than 8µm, which were in accordance with the CTC criterion. In Figure 3B, the magnetic ball was stained with blue by prussian blue.

Recognition of CTCs between EpCAM magnetic ball and EILs

Blood samples from 7 cases of colorectal cancer patients without chemotherapy were collected for CTC capture count analysis. For each patient, 7.5 mL of blood was divided equally for identifying CTC number by EpCAM and EILs.The number of CTCs identified by EpCAM magnetic ball was 15 to 79 and by EILs was 5 to 181. A significant difference was found between two methods. As shown in Figure 4, we could see that numbers in patient 1, 2, 4, 5, 6 and 7 by EILs were higher than those by EpCAM magnetic ball.

Mutations analysis in CTCs

KRAS has been recognized as a marker for diagnosis and treatment of colorectal cancer. Mutations of KRAS in CTCs from the 7 colorectal cancer patients were compared. 5 of the 7 DNA samples were successfully amplified and sequenced. We further amplified and sequenced their DNA of tumor tissue, and found they were coincident (Figure 5 and Table 1).

Discussion

In current study, we describeda newly constructed EGFR immune magnetic liposomes (EILs) for capturing colorectal CTCs. The results found that EILs showed similarity with cell membrane and could more efficiently capture colorectal CTCs compared with EpCAM immunomagnetic beads.

The relatively higher efficiency of EILs compared to EpCAM immunomagnetic beads might be explained by the following facts. Firstly, the obtained IML displayed a lipid nanoparticle structure similar tocell membrane which enhancedcontact with cancer cells[33-35]. Secondly, Characterizations of the EILs was similar to IML (including mean hydrodynamic size, Zeta potential, magnetization curves and saturation magnetization value), which suggested EILs could effectively combine CTC cells[30,32,36]. Thirdly, expression of EpCAM on CTCs is dynamic[24,37]. Some cells might not express EpCAM and did not get captured[22,38,39].

Meanwhile, we could not ignore that in one patient, the number of CTCs captured by EILs was lower than those by EpCAM magnetic ball. This patient was in stage I and the number of CTCs in the peripheral blood might bemuch fewer than those at advanced stages which fell below the detection limit of EILs. Other factor such as operating mistakes or an isolated phenomenon might also be an explanation. More studies with larger quantity of cases included were needed to validate current findings.

The feasibility of CTCs captured by EILs was evaluated by mutation analysis, especially KRAS gene. 5 of the 7 DNA samples were successfully amplified and sequenced, and compared to mutations in tumor tissue. We found that mutation in CTCs and tumor tissues were the same. Considering that KRAS was reported to be a marker for diagnosis and predicting treatment outcomes of colorectal cancer[28,40-42], the current results suggested that detecting CTCs KRAS mutations through EILs capture and gene detection might be of practical use.

In 2005, Kullberg and colleagues firstly reported the use of magnetic liposomes modified by EGFR antibody for drug delivery to cancer cells[31]. Recently, Wang et al[43] found that magnetic liposomes modified by dual antibody (the nuclear protein Ki-67 and EGFR antibody) was potentially useful in helping treat tumor cells with proliferative characteristics. Our current study further confirmed the feasibility of EILs in capturing CTCs. These findings suggested that EGFR magnetic liposomes might be of more clinical significance in the future.

There were at least two limitations that should be paid attention to. Firstly, the number of patients included in our study is small. Secondly, all of the colorectal cancer patients included in the study were EGFR positive which might cause a great bias to our results as previous study reported that the sensitivity and specificity of EGFR were lower than EpCAM for colorectal cancer patients[44]. Liu et al[45] also reported that the positive expression rate of EGFR was only 64% (45/70). Future studies might include several specific molecular targets to improve efficiency[46]. For example, Myung et al[47] successfully enhanced tumor cell isolation by a biomimetic combination of E-selectin and anti-EpCAM. Besides, combing mechanical and molecular filtration seemed another possibility to better enrichment of CTCs[48-51].

In conclusion, we designed a new CTC-capture platform that combines a high-affinity cell enrichment assay based on cell capture-agent (antibody)-coated nanostructured substrates and a cell membrane structure capable of improving CTC/substrate contact frequency.The synergistic effects led to better CTC-capture performance in clinical blood samples compared with traditional EpCAM immunomagnetic beads. The significantly improved sensitivity of our new CTC capture technology might be useful in early detection of cancer metastasis and isolation of rare populations of cells.

ARTICLE HIGHLIGHTS

Research background

Metastasis contributes most to cancer-related deaths in patients with solid tumors. Mounting evidences suggested circulating tumor cells (CTCs) which can shed from a primary tumor massat the earliest stages of malignant progression played a critical role in cancer metastasis. Detection and characterization of CTCs is challenging owing to their extreme scarcity in blood. However, the sensitivity of aforementioned methods relies greatly on the enrichment degree of CTCs and current techniques used is far from satisfactory. Recently, a new method in which a cell bilayer membrane structured magnetic liposome prepared directly with cancer-cell capture agents-epidermal growth factor receptor (EGFR) antibody was discovered. Studies found a significant improvement in cell-capture efficiency owing to its enhanced interactions between the deformable antibody receptor-lipid bilayer structure and nanoscale cellular surface components. Such a high-affinity cell assay can be employed to recover cancer cells from spiked whole-blood samples, in stationary magnetic separation device by anti-EGFR magnetic nano-vesicles.

Research motivation

The main topics are to compare the capture capacityof newly self-constructed EGFR immune magnetic liposomes (EILs) on colorectal circulating tumor cells(CTCs)with that of epithelial cell adhesion molecule (EpCAM) immunomagnetic beads.

Research objectives

The main objectives are to compare the capture capacityof newly self-constructed EGFR immune magnetic liposomes (EILs) on colorectal circulating tumor cells (CTCs) with that of epithelial cell adhesion molecule (EpCAM) immunomagnetic beads. And the significantly improved sensitivity of our new CTC capture technology might be useful in early detection of cancer metastasis and isolation of rare populations of cells.

Research methods

EILs was constructed using a two-step synthesis method and the magnetic and surface characterizations were confirmed. The capture efficiency on colorectal CTCs as well as the specificitywere compared between EILs and EpCAM magnetic ball. Statistical analysis was carried out by Prism software (GraphPad Software, Inc., La Jolla, CA). The unpaired Student’s t-test was used to compare hydrodynamic size, diffuse efficient and zeta potential between IML and EILs. A paired Student’s t-test was used to detect differences in the number of CTC captured by EpCAM immunomagnetic beads in comparison with EILs. A P value of smaller than 0.05 was considered to be statistically significant.

Research results

The obtained EILs have a lipid nanoparticle structure similar to cell membrane. An improved combination with cancer cells was seen in EILs compared with the modification method of combining antibody to nano/microspheres. The combination increased as the contact time extended. Compared with EpCAM immunomagnetic beads, EILs captured more CTCs in blood of colorectalcancer patients.The captured cells showed consistency with clinical diagnosis and pathology. Mutation analysis showed same results between captured CTCs and cancer tissues.

Research conclusions

An improved combination with cancer cells was seen in EILs compared with the modification method of combining antibody to nano/microspheres. EILs was constructed using a two-step synthesis method and the magnetic and surface characterizations were confirmed. The capture efficiency on colorectal CTCs as well as the specificity were compared between EILs and EpCAM magnetic ball. Using a two-step synthesis method and the magnetic and surface characterizations were confirmed. EGFR coated with magnetic liposomes showed high efficiency and specificity in the capture of colorectal CTCs. The captured cells showed consistency with clinical diagnosis and pathology. Mutation analysis showed same results between captured CTCs and cancer tissues. EILs was constructed using a two-step synthesis method and the magnetic and surface characterizations were confirmed. The capture efficiency on colorectal CTCs as well as the specificitywere compared between EILs and EpCAM magnetic ball. EGFR coated with magnetic liposomes showed high efficiency and specificity in the capture of colorectal CTCs. The significantly improved sensitivity of our new CTC capture technology might be useful in early detection of cancer metastasis and isolation of rare populations of cells.

Research perspectives

Everything must be on bases of this stationary cell-capture assay. The significantly improved sensitivity of our new CTC capture technology might be useful in early detection of cancer metastasis and isolation of rare populations of cells. Cancer metastasis and isolation of rare populations of cells

ReferenceS

1 Pantel K, Speicher MR. The biology of circulating tumor cells. Oncogene 2016; 35: 1216-1224 [PMID: 26050619 DOI: 10.1038/onc.2015.192]

2 Joosse SA, Gorges TM, Pantel K. Biology, detection, and clinical implications of circulating tumor cells. EMBO Mol Med 2015; 7: 1-11 [PMID: 25398926 DOI: 10.15252/emmm.201303698]

3 Hardingham JE, Grover P, Winter M, Hewett PJ, Price TJ, Thierry B. Detection and Clinical Significance of Circulating Tumor Cells in Colorectal Cancer--20 Years of Progress. Mol Med 2015; 21 Suppl 1: S25-S31 [PMID: 26605644 DOI: 10.2119/molmed.2015.00149]

4 Li N, Xiao T, Zhang Z, He R, Wen D, Cao Y, Zhang W, Chen Y. A 3D graphene oxide microchip and a Au-enwrapped silica nanocomposite-based supersandwich cytosensor toward capture and analysis of circulating tumor cells. Nanoscale 2015; 7: 16354-16360 [PMID: 26391313 DOI: 10.1039/c5nr04798f]

5 Rink M, Chun FK, Dahlem R, Soave A, Minner S, Hansen J, Stoupiec M, Coith C, Kluth LA, Ahyai SA, Friedrich MG, Shariat SF, Fisch M, Pantel K, Riethdorf S. Prognostic role and HER2 expression of circulating tumor cells in peripheral blood of patients prior to radical cystectomy: a prospective study. Eur Urol 2012; 61: 810-817 [PMID: 22277196 DOI: 10.1016/j.eururo.2012.01.017]

6 Jansson S, Bendahl PO, Larsson AM, Aaltonen KE, Rydén L. Prognostic impact of circulating tumor cell apoptosis and clusters in serial blood samples from patients with metastatic breast cancer in a prospective observational cohort. BMC Cancer 2016; 16: 433 [PMID: 27390845 DOI: 10.1186/s12885-016-2406-y]

7 Gazzaniga P, Raimondi C, Nicolazzo C, Carletti R, di Gioia C, Gradilone A, Cortesi E. The rationale for liquid biopsy in colorectal cancer: a focus on circulating tumor cells. Expert Rev Mol Diagn 2015; 15: 925-932 [PMID: 25959553 DOI: 10.1586/14737159.2015.1045491]

8 Lee GW, Kim JY, Koh EH, Kang D, Choi DS, Maeng KY, Lee JS. Plasma human mammaglobin mRNA associated with poor outcome  in patients with breast cancer. Genet Mol Res 2012; 11: 4034-4042 [PMID: 23212340 DOI: 10.4238/2012.November.28.2]

9 Alix-Panabières C, Pantel K. Technologies for detection of circulating tumor cells: facts and vision. Lab Chip 2014; 14: 57-62 [PMID: 24145967 DOI: 10.1039/c3lc50644d]

10 Chen JF, Zhu Y, Lu YT, Hodara E, Hou S, Agopian VG, Tomlinson JS, Posadas EM, Tseng HR. Clinical Applications of NanoVelcro Rare-Cell Assays for Detection and Characterization of Circulating Tumor Cells. Theranostics 2016; 6: 1425-1439 [PMID: 27375790 DOI: 10.7150/thno.15359]

11 Lin M, Chen JF, Lu YT, Zhang Y, Song J, Hou S, Ke Z, Tseng HR. Nanostructure embedded microchips for detection, isolation, and characterization of circulating tumor cells. Acc Chem Res 2014; 47: 2941-2950 [PMID: 25111636 DOI: 10.1021/ar5001617]

12 Lu Y, Liang H, Yu T, Xie J, Chen S, Dong H, Sinko PJ, Lian S, Xu J, Wang J, Yu S, Shao J, Yuan B, Wang L, Jia L. Isolation and characterization of living circulating tumor cells in patients by immunomagnetic negative enrichment coupled with flow cytometry. Cancer 2015; 121: 3036-3045 [PMID: 25945459 DOI: 10.1002/cncr.29444]

13 Qian W, Zhang Y, Chen W. Capturing Cancer: Emerging Microfluidic Technologies for the Capture and Characterization of Circulating Tumor Cells. Small 2015; 11: 3850-3872 [PMID: 25993898 DOI: 10.1002/smll.201403658]

14 Zheng S, Lin HK, Lu B, Williams A, Datar R, Cote RJ, Tai YC. 3D microfilter device for viable circulating tumor cell (CTC) enrichment from blood. Biomed Microdevices 2011; 13: 203-213 [PMID: 20978853 DOI: 10.1007/s10544-010-9485-3]

15 Ankeny JS, Court CM, Hou S, Li Q, Song M, Wu D, Chen JF, Lee T, Lin M, Sho S, Rochefort MM, Girgis MD, Yao J, Wainberg ZA, Muthusamy VR, Watson RR, Donahue TR, Hines OJ, Reber HA, Graeber TG, Tseng HR, Tomlinson JS. Circulating tumour cells as a biomarker for diagnosis and staging in pancreatic cancer. Br J Cancer 2016; 114: 1367-1375 [PMID: 27300108 DOI: 10.1038/bjc.2016.121]

16 Wang FB, Yang XQ, Yang S, Wang BC, Feng MH, Tu JC. A higher number of circulating tumor cells (CTC) in peripheral blood indicates poor prognosis in prostate cancer patients--a meta-analysis. Asian Pac J Cancer Prev 2011; 12: 2629-2635 [PMID: 22320965]

17 Barriere G, Riouallon A, Renaudie J, Tartary M, Rigaud M. Mesenchymal characterization: alternative to simple CTC detection in two clinical trials. Anticancer Res 2012; 32: 3363-3369 [PMID: 22843916]

18 Karl A, Tritschler S, Hofmann S, Stief CG, Schindlbeck C. Perioperative search for circulating tumor cells in patients undergoing radical cystectomy for bladder cancer. Eur J Med Res 2009; 14: 487-490 [PMID: 19948444]

19 Coumans F, Terstappen L. Detection and Characterization of Circulating Tumor Cells by the CellSearch Approach. Methods Mol Biol 2015; 1347: 263-278 [PMID: 26374323 DOI: 10.1007/978-1-4939-2990-0_18]

20 Huang X, Gao P, Song Y, Sun J, Chen X, Zhao J, Xu H, Wang Z. Meta-analysis of the prognostic value of circulating tumor cells detected with the CellSearch System in colorectal cancer. BMC Cancer 2015; 15: 202 [PMID: 25880692 DOI: 10.1186/s12885-015-1218-9]

21 Steinarsdóttir M, Jónasson JG, Vidarsson H, Júlíusdóttir H, Hauksdóttir H, Ogmundsdóttir HM. Cytogenetic changes in nonmalignant breast tissue. Genes Chromosomes Cancer 2004; 41: 47-55 [PMID: 15236316 DOI: 10.1002/gcc.20055]

22 Gorges TM, Tinhofer I, Drosch M, Röse L, Zollner TM, Krahn T, von Ahsen O. Circulating tumour cells escape from EpCAM-based detection due to epithelial-to-mesenchymal transition. BMC Cancer 2012; 12: 178 [PMID: 22591372 DOI: 10.1186/1471-2407-12-178]

23 Grover PK, Cummins AG, Price TJ, Roberts-Thomson IC, Hardingham JE. Circulating tumour cells: the evolving concept and the inadequacy of their enrichment by EpCAM-based methodology for basic and clinical cancer research. Ann Oncol 2014; 25: 1506-1516 [PMID: 24651410 DOI: 10.1093/annonc/mdu018]

24 Gires O, Stoecklein NH. Dynamic EpCAM expression on circulating and disseminating tumor cells: causes and consequences. Cell Mol Life Sci 2014; 71: 4393-4402 [PMID: 25103341 DOI: 10.1007/s00018-014-1693-1]

25 Sieuwerts AM, Kraan J, Bolt J, van der Spoel P, Elstrodt F, Schutte M, Martens JW, Gratama JW, Sleijfer S, Foekens JA. Anti-epithelial cell adhesion molecule antibodies and the detection of circulating normal-like breast tumor cells. J Natl Cancer Inst 2009; 101: 61-66 [PMID: 19116383 DOI: 10.1093/jnci/djn419]

26 Diepenbruck M, Christofori G. Epithelial-mesenchymal transition (EMT) and metastasis: yes, no, maybe? Curr Opin Cell Biol 2016; 43: 7-13 [PMID: 27371787 DOI: 10.1016/j.ceb.2016.06.002]

27 Limasale YD, Tezcaner A, Özen C, Keskin D, Banerjee S. Epidermal growth factor receptor-targeted immunoliposomes for delivery of celecoxib to cancer cells. Int J Pharm 2015; 479: 364-373 [PMID: 25595386 DOI: 10.1016/j.ijpharm.2015.01.016]

28 Baas JM, Krens LL, Guchelaar HJ, Morreau H, Gelderblom H. Concordance of predictive markers for EGFR inhibitors in primary tumors and metastases in colorectal cancer: a review. Oncologist 2011; 16: 1239-1249 [PMID: 21742964 DOI: 10.1634/theoncologist.2011-0024]

29 Zhai J, Scoble JA, Li N, Lovrecz G, Waddington LJ, Tran N, Muir BW, Coia G, Kirby N, Drummond CJ, Mulet X. Epidermal growth factor receptor-targeted lipid nanoparticles retain self-assembled nanostructures and provide high specificity. Nanoscale 2015; 7: 2905-2913 [PMID: 25516406 DOI: 10.1039/c4nr05200e]

30 Nobuto H, Sugita T, Kubo T, Shimose S, Yasunaga Y, Murakami T, Ochi M. Evaluation of systemic chemotherapy with magnetic liposomal doxorubicin and a dipole external electromagnet. Int J Cancer 2004; 109: 627-635 [PMID: 14991586 DOI: 10.1002/ijc.20035]

31 Kullberg M, Mann K, Owens JL. Improved drug delivery to cancer cells: a method using magnetoliposomes that target epidermal growth factor receptors. Med Hypotheses 2005; 64: 468-470 [PMID: 15617850 DOI: 10.1016/j.mehy.2004.07.033]

32 Kulshrestha P, Gogoi M, Bahadur D, Banerjee R. In vitro application of paclitaxel loaded magnetoliposomes for combined chemotherapy and hyperthermia. Colloids Surf B Biointerfaces 2012; 96: 1-7 [PMID: 22521681 DOI: 10.1016/j.colsurfb.2012.02.029]

33 Onuki Y, Obata Y, Kawano K, Sano H, Matsumoto R, Hayashi Y, Takayama K. Membrane Microdomain Structures of Liposomes and Their Contribution to the Cellular Uptake Efficiency into HeLa Cells. Mol Pharm 2016; 13: 369-378 [PMID: 26709741 DOI: 10.1021/acs.molpharmaceut.5b00601]

34 Liang X, Shi B, Wang K, Fan M, Jiao D, Ao J, Song N, Wang C, Gu J, Li Z. Development of self-assembling peptide nanovesicle with bilayers for enhanced EGFR-targeted drug and gene delivery. Biomaterials 2016; 82: 194-207 [PMID: 26763734 DOI: 10.1016/j.biomaterials.2015.12.015]

35 Fleischer CC, Payne CK. Nanoparticle-cell interactions: molecular structure of the protein corona and cellular outcomes. Acc Chem Res 2014; 47: 2651-2659 [PMID: 25014679 DOI: 10.1021/ar500190q]

36 Moghimi SM, Hunter AC, Murray JC. Long-circulating and target-specific nanoparticles: theory to practice. Pharmacol Rev 2001; 53: 283-318 [PMID: 11356986]

37 Driemel C, Kremling H, Schumacher S, Will D, Wolters J, Lindenlauf N, Mack B, Baldus SA, Hoya V, Pietsch JM, Panagiotidou P, Raba K, Vay C, Vallböhmer D, Harréus U, Knoefel WT, Stoecklein NH, Gires O. Context-dependent adaption of EpCAM expression in early systemic esophageal cancer. Oncogene 2014; 33: 4904-4915 [PMID: 24141784 DOI: 10.1038/onc.2013.441]

38 Shigdar S, Qian C, Lv L, Pu C, Li Y, Li L, Marappan M, Lin J, Wang L, Duan W. The use of sensitive chemical antibodies for diagnosis: detection of low levels of EpCAM in breast cancer. PLoS One 2013; 8: e57613 [PMID: 23460885 DOI: 10.1371/journal.pone.0057613]

39 Yoshida GJ, Saya H. EpCAM expression in the prostate cancer makes the difference in the response to growth factors. Biochem Biophys Res Commun 2014; 443: 239-245 [PMID: 24309103 DOI: 10.1016/j.bbrc.2013.11.093]

40 Alves S, Castro L, Fernandes MS, Francisco R, Castro P, Priault M, Chaves SR, Moyer MP, Oliveira C, Seruca R, Côrte-Real M, Sousa MJ, Preto A. Colorectal cancer-related mutant KRAS alleles function as positive regulators of autophagy. Oncotarget 2015; 6: 30787-30802 [PMID: 26418750 DOI: 10.18632/oncotarget.5021]

41 Chang YY, Lin JK, Lin TC, Chen WS, Jeng KJ, Yang SH, Wang HS, Lan YT, Lin CC, Liang WY, Chang SC. Impact of KRAS mutation on outcome of patients with metastatic colorectal cancer. Hepatogastroenterology 2014; 61: 1946-1953 [PMID: 25713893]

42 Therkildsen C, Bergmann TK, Henrichsen-Schnack T, Ladelund S, Nilbert M. The predictive value of KRAS, NRAS, BRAF, PIK3CA and PTEN for anti-EGFR treatment in metastatic colorectal cancer: A systematic review and meta-analysis. Acta Oncol 2014; 53: 852-864 [PMID: 24666267]

43 Wang S, Hüttmann G, Scholzen T, Zhang Z, Vogel A, Hasan T, Rahmanzadeh R. A light-controlled switch after dual targeting of proliferating tumor cells via the membrane receptor EGFR and the nuclear protein Ki-67. Sci Rep 2016; 6: 27032 [PMID: 27246531 DOI: 10.1038/srep27032]

44 Mourtzikou A, Stamouli M, Kroupis C, Christodoulou S, Skondra M, Kastania A, Pectasides D, Athanasas G, Dimas C. Evaluation of carcinoembryonic antigen (CEA), epidermal growth factor receptor (EGFR), epithelial cell adhesion molecule EpCAM (GA733-2), and carbohydrate antigen 19-9 (CA 19-9) levels in colorectal cancer patients and correlation with clinicopathological characteristics. Clin Lab 2012; 58: 441-448 [PMID: 22783573]

45 Liu J, Zhou Q, Xu J, Wang J, Zhang Y. Detection of EGFR expression in patients with colorectal cancer and the therapeutic effect of cetuximab. J BUON 2016; 21: 95-100 [PMID: 27061536]

46 Gorges TM, Stein A, Quidde J, Hauch S, Röck K, Riethdorf S, Joosse SA, Pantel K. Improved Detection of Circulating Tumor Cells in Metastatic Colorectal Cancer by the Combination of the CellSearch® System and the AdnaTest®. PLoS One 2016; 11: e0155126 [PMID: 27182774 DOI: 10.1371/journal.pone.0155126]

47 Myung JH, Launiere CA, Eddington DT, Hong S. Enhanced tumor cell isolation by a biomimetic combination of E-selectin and anti-EpCAM: implications for the effective separation of circulating tumor cells (CTCs). Langmuir 2010; 26: 8589-8596 [PMID: 20155985 DOI: 10.1021/la904678p]

48 Meunier A, Hernández-Castro JA, Turner K, Li K, Veres T, Juncker D. Combination of Mechanical and Molecular Filtration for Enhanced Enrichment of Circulating Tumor Cells. Anal Chem 2016; 88: 8510-8517 [PMID: 27442305 DOI: 10.1021/acs.analchem.6b01324]

49 Bhana S, Wang Y, Huang X. Nanotechnology for enrichment and detection of circulating tumor cells. Nanomedicine (Lond) 2015; 10: 1973-1990 [PMID: 26139129 DOI: 10.2217/nnm.15.32]

50 Hanssen A, Wagner J, Gorges TM, Taenzer A, Uzunoglu FG, Driemel C, Stoecklein NH, Knoefel WT, Angenendt S, Hauch S, Atanackovic D, Loges S, Riethdorf S, Pantel K, Wikman H. Characterization of different CTC subpopulations in non-small cell lung cancer. Sci Rep 2016; 6: 28010 [PMID: 27302574 DOI: 10.1038/srep28010]

51 Tulley S, Zhao Q, Dong H, Pearl ML, Chen WT. Vita-Assay™ Method of Enrichment and Identification of Circulating Cancer Cells/Circulating Tumor Cells (CTCs). Methods Mol Biol 2016; 1406: 107-119 [PMID: 26820949 DOI: 10.1007/978-1-4939-3444-7_9]

P-Reviewer: Kane S, McCarthy M, Provenzale D S-Editor: Ma YJ L-Editor:   E-Editor:

Specialty type: Gastroenterology and hepatology

Country of origin: China

Peer-review report classification

Grade A (Excellent): A

Grade B (Very good): B

Grade C (Good): C

Grade D (Fair): 0

Grade E (Poor): 0

Table 1 Comparison gene mutant of circulating tumor cells DNA with plasma DNA

| Sample ID | Tumo r type | Clinical stage | CTCs DNA | Tissue DNA |
| --- | --- | --- | --- | --- |
|  |  |  | KRAS Exon 1 | KRAS Exon 2 | KRAS Exon 1 | KRAS Exon 2 |
| 1 | Colorectalcancer | IV | WT | WT | WT | WT |
| 2 | Colorectalcancer | Ⅲ | WT | WT | WT | WT |
| 3 | Colorectalcancer | I | NAP | NAP | WT | WT |
| 4 | Colorectalcancer | IV | WT | WT | WT | WT |
| 5 | Colorectalcancer | IV | WT | WT | WT | WT |
| 6 | Colorectalcancer | II | NAP | NAP | WT | WT |
| 7 | Colorectalcancer | III | WT | WT | WT | WT |

CTCs: circulating tumor cells; WT: wild type; NAP: not amplified.

Figure 1 Schematic diagram showing the preparation of epidermal growth factor receptor immune magnetic liposomes with hydrophilic and hydrophobic magnetic nanoparticles. EGFR: epidermal growth factor receptor.

Figure 2 Characterization of epidermal growth factor receptor immune magnetic liposomes. The hydrodynamic diameter (A), Zeta potential (B) and Magnetization curves (C) at 300 K of magnetic polymeric liposomes. IML: immune magnetic liposomes; EGFR: epidermal growth factor receptor; EILs, EGFR immune magnetic liposomes.

Figure 3 Size of the captured circulating tumor cells cells and color of stained magnetic ball. A: Localization and distribution of EILs in HT-29 cells. Cells were cultured in FITC-labeled EILs-containing medium on bottom of glass dish (35 mm dish with 14 mm bottom well) for 30 min followed by treatment with DAPI dyes and Dil dyes for 5-10 min separately, and subsequent examination by confocal microscopy; B: Prussian blue staining of EGFR IML with HT-29 Cells. (Scale bar: 5 µm). IML: immune magnetic liposomes; EILs: EGFR immune magnetic liposomes.

Figure 4 The number of circulating tumor cells identified by epithelial cell adhesion molecule magnetic and epidermal growth factor receptor immune magnetic liposomes. Side-by-side representation of circulating tumor cell (CTC) enumeration results obtained from our integrated CTC-capture method (normalized to 7.5 mL of blood) with EGFR immune magnetic liposomes and epithelial cell adhesion molecule (EpCAM) immunomagnetic beads on matched samples from 7 patients, and by EpCAM magnetic ball was 15 to 79 and by epidermal growth factor receptor immune magnetic liposomes (EILs) was 5 to 181.

Figure 5 Gene mutation test of KRAS for captured circulating tumor cells and tumor tissue. CTCs: circulating tumor cells.