| Biodegradable stents in gastrointestinal endoscopy Vicente Lorenzo-Zúñiga, Vicente Moreno-de-Vega, Ingrid Marín, Jaume Boix |
| --- |
| CITATION | Lorenzo-Zúñiga V, Moreno-de-Vega V, Marín I, Boix J. Biodegradable stents in gastrointestinal endoscopy. World J Gastroenterol 2014; 20(9): 2212-2217 |
| URL | http://www.wjgnet.com/1007-9327/full/v20/i9/2212.htm |
| DOI | http://dx.doi.org/10.3748/wjg.v20.i9.2212 |
| OPEN ACCESS | Articles published by this Open-Access journal are distributed under the terms of the Creative Commons Attribution Non-commercial License, which permits use, distribution, and reproduction in any medium, provided the original work is properly cited, the use is non commercial and is otherwise in compliance with the license. |
| CORE TIP | The experience with the currently the only biodegradable stents (BDSs) for endoscopic placement, made of poly-dioxanone, have shown promising results. However some aspects should be improved as are the fact that BDSs lose their radial force over time due to the degradable material, and that can cause stent-induced mucosal or parenchymal injury. This complication rate and modest clinical efficacy has to be carefully considered in individual patients prior to placement of BDSs. Otherwise, the price of these stents therefore it is nowadays an important limitation. |
| KEY WORDS | Biodegradable stents; Strictures; Endoscopy; Endoscopic placement; Stenoses |
| COPYRIGHT | © 2014 Baishideng Publishing Group Co., Limited. All rights reserved. |
| COPYRIGHT LICENSE | Order reprints or request permissions: bpgoffice@wjgnet.com |
| NAME OF JOURNAL | World Journal of Gastroenterology |
| ISSN | 1007-9327 (print) 2219-2840 (online) |
| PUBLISHER | Baishideng Publishing Group Co., Limited, Flat C, 23/F., Lucky Plaza, 315-321 Lockhart Road, Wan Chai, Hong Kong, China |
| WEBSITE | http://www.wjgnet.com |

Name of journal: World Journal of Gastroenterology

ESPS Manuscript NO: 5613

Columns: TOPIC HIGHLIGHT

Biodegradable stents in gastrointestinal endoscopy

Vicente Lorenzo-Zúñiga, Vicente Moreno-de-Vega, Ingrid Marín, Jaume Boix

Vicente Lorenzo-Zúñiga, Vicente Moreno-de-Vega, Ingrid Marín, Jaume Boix, Endoscopy Unit, Department of Gastroenterology, Hospital Universitari Germans Trias i Pujol, 08916 Badalona, Spain

Vicente Lorenzo-Zúñiga, Centro de Investigación Biomédica en Red de Enfermedades Hepáticas y Digestivas (CIBEREHD), 08916 Badalona, Spain

Author contributions: Lorenzo-Zúñiga V was involved in editing the manuscript and wrote the manuscript; Moreno-de-Vega V, Marín I and Boix J revised the manuscript.

Correspondence to: Vicente Lorenzo-Zúñiga, MD, PhD, Endoscopy Unit, Department of Gastroenterology, Hospital Universitari Germans Trias i Pujol, Carretera del Canyet s/n. 08916 Badalona, Spain. vlorenzo.germanstrias@gencat.cat

Telephone: +34-93-4978866     Fax: +34-93-4978866

Received: September 17, 2013  Revised: November 2, 2013  Accepted: December 3, 2013

Published online: March 7, 2014

Abstract

Biodegradable stents (BDSs) are an attractive option to avoid ongoing dilation or surgery in patients with benign stenoses of the small and large intestines. The experience with the currently the only BDS for endoscopic placement, made of Poly-dioxanone, have shown promising results. However some aspects should be improved as are the fact that BDSs lose their radial force over time due to the degradable material, and that can cause stent-induced mucosal or parenchymal injury. This complication rate and modest clinical efficacy has to be carefully considered in individual patients prior to placement of BDSs. Otherwise, the price of these stents therefore it is nowadays an important limitation.

© 2014 Baishideng Publishing Group Co., Limited. All rights reserved.

Key words: Biodegradable stents; Strictures; Endoscopy; Endoscopic placement; Stenoses

Core tip: The experience with the currently the only biodegradable stents (BDSs) for endoscopic placement, made of poly-dioxanone, have shown promising results. However some aspects should be improved as are the fact that BDSs lose their radial force over time due to the degradable material, and that can cause stent-induced mucosal or parenchymal injury. This complication rate and modest clinical efficacy has to be carefully considered in individual patients prior to placement of BDSs. Otherwise, the price of these stents therefore it is nowadays an important limitation.

Lorenzo-Zúñiga V, Moreno-de-Vega V, Marín I, Boix J. Biodegradable stents in gastrointestinal endoscopy. World J Gastroenterol 2014; 20(9): 2212-2217  Available from: URL: http://www.wjgnet.com/1007-9327/full/v20/i9/2212.htm  DOI: http://dx.doi.org/10.3748/wjg.v20.i9.2212

INTRODUCTION

Metal and plastic stents are an effective treatment to manage both benign and malignant strictures throughout the gastrointestinal (GI) tract; however, the use of these stents is associated with several common problems including migration, tissue ingrowths and repetitive endoscopic procedures. During the last two decades, significant advances have been made in the development of biocompatible and biodegradable materials for medical applications, and to overcome those shortcomings, stents made of biodegradable materials have been developed. The cardiovascular stent market is the dominant driving force for research and development of biodegradable stents (BDSs)[1]. In the GI tract much less is currently known about the clinical utility and the experience with these stents.

BIOMATERIALS

Biomaterial is a non-living material used in a medical device and designed to interact with biological systems. Biomaterial can be (1) inert, do not trigger any reaction in the host; (2) bioactive, ensure a more stable performance in a long time or for the period you want; or (3) biodegradable, it can be chemically degraded or decomposed by natural effectors as bacteria. The mean features of these materials for medical applications are absence of carcinogenicity, immunogenicity, teratogenicity and toxicity.

More used biomaterials are magnesium alloys based and synthetic polymers: poly-lactic acid (PLA), poly-glycolic acid (PGA), poly-caprolactone (PCL), poly-dioxanone (PDX) and poly-lactide-co-glycolide.

Main advantages of magnesium alloys based are high biocompatibility and property to be dissolved into human body during the degradation process; however, due to this high corrosion rate, degradation occurs before the end of healing process.

Polymers degrade slower than magnesium alloys. Most polymers used in medical devices allow the spread of water within molecular structure and can therefore result in processes hydrolysis. The ideal polymer should be: (1) sufficiently strong until surrounding tissue has healed; (2) does not invoke inflammatory or toxic response; (3) to be metabolized in the body after fulfilling its purpose; (4) leaving no trace to be easily processable into the final product form; (5) must demonstrates acceptable shelf life; and (6) to be easily sterilized. With these characteristics; the main advantages of synthetic polymers are: (1) good biocompatibility; (2) possibility of changing in composition and in physical-mechanical properties; (3) low coefficients of friction; (4) easy processing and workability; (5) ability to change surface chemically and physically; and (6) ability to immobilize cells or biomolecules within them or on the surface (Drug Eluting Stent). Biodegradable polymers used for drug release represent the next technological modification and preliminary results are favorable in vascular system and clinical efficacy as first-generation drug eluting stent, but gastrointestinal application has not been reported yet[2].

According to these features, BDS can be made of different synthetic polymers (PLA, PGA) or their co-polymers (PDX). Their degradation is hydrolytic and the speed of biodegradation is dependent not only on the size and structure, but also influenced by temperature, pH and type of body tissue/fluid[3,4].

CLINICAL EXPERIENCE

The first report was published in 1993[5] in an experimental model of urethral stenosis with rabbits treated with a stent made of PLA. In gastrointestinal endoscopy, BDSs made of PLA were developed by Goldin et al[6], who reported their experience with five patients with benign esophageal strictures. These authors described that this prototype did not maintain significantly radial force over a 3-wk period, and disintegrated 6 wk later and obstructed the esophageal lumen, data that was confirmed by another group[7].

BDSs made of PDX have improved the results because stent integrity and radial force can be maintained for 6-8 wk after implantation[8]. In this pilot study with three patients with benign tight small and large intestinal stenoses, the authors confirmed that stent degradation and fragmentation occurs 11-12 wk after its insertion; otherwise, the speed of degradation is pH-dependent (faster in lower pH).

The prolonged dilatory effect before stent absorption and the progressive stent degradation could represent a more favorable solution for patients with benign strictures refractory to standard dilation therapy compared with self-expandable metal and plastic stents. These newly stents allow for constant radial dilation, similar to date achieved by a metallic stent, but with the advantage that they do not have to be removed. To date, PDX-BDSs could be an alternative for benign refractory strictures in the GI tract.

Esophagus

Placement of BDS is an emerging and promising treatment alternative for benign esophageal strictures and achalasia. These strictures are often caused by esophageal reflux, the ingestion of caustic substances, esophageal surgery and radiation therapy[9]. Endoscopic dilation using bougies or balloons has been established as a standard therapy, and it is associated with an immediate 80%-90% success rate of relieving dysphagia[10]. However, 30%-60% of benign strictures will recur during long-term follow-up; thus, an alternative treatment strategy should be considered[11].

BDSs have recently been developed. Initially, these stents were made of PLA, with a configuration and mechanical radial force similar to those commercially available esophageal stents[12]. Saito et al[13,14] reported results from two series of patients who received this type of PLA esophageal stents, but the majority (77%) of stents had migrated out of the esophagus within 10-21 d of insertion, although clinical success was observed in all cases within the follow-up period of 7 mo to 2 years.

Another novel stent (Ella esophageal stent) composed of the biodegradable polymer PDX has become to be used from 2007 (and currently the only). This stent is assembled onto a 9.4-mm (28 F) delivery system, and comes in several sizes, with stent body diameters ranging from 18 to 25 mm and fully deployed lengths of 60-135 mm. Integrity and radial force are completely maintained for approximately 6 wk following implantation. From 7-9 wk is 2/3 of the initial, after the 9 wk is 1/3, and the average time to complete degradation of the stent is reported to be 11-12 wk[8]. Acid-suppressing therapy is recommended, because more rapid degradation occurs with acid exposure.

Published experience has been reported with the SX-ELLA-BD stent for treatment of refractory benign esophageal strictures (RBES)[9,15-29] as well as achalasia[30] (Table 1). Technical success, clinical responses and outcomes were varied. Stent implantation is not a problem, but clinical success ranged from 0 to 100, with a mean of 39.4%. The largest long-term follow-up series of BDSs placement in 28 patients with RBES were reported by Hirdes et al[22], with a clinical success rate after the first BDS placement of 25%.

To avoid complications of partially covered/uncovered stents, temporary placement of 3 different types of expandable stents have been used for the treatment of RBES: self-expanding plastic stents (SEPSs), BDSs and fully covered self-expandable metal stents (FC-SEMSs). To date there is only one published study that compares the efficacy of these three types of stent for the treatment of RBES[9]. These authors showed that temporary placement of BDSs or FC-SEMSs have similar utility in the treatment of RBES, with a long-term dysphagia-free period in 30% and 40% of patients, respectively. The use of SEPSs were associated with the worst clinical success rate (10%) as well as with a higher number of migrations and reinterventions. A long stricture was the only significant fact associated with a higher recurrence rate after stent placement. Migration rate was higher with FC-SEMSs (30%) than with BDSs (20%). The implementation of balloon dilatation of the BDS stent after deployment did decrease migration rated compared to before balloon dilation.

Thoracic pain is the most frequent complication reported in the literature. Hyperplasic tissue reaction occurs in conjunction with stent degradation and the severity of the tissue response and the time to complete degradation, both important factors when considering patients for placement of a BDS, are still well not understood. Cases of severe tissue hyperplasia resulting in recurrent dysphagia have been described[16,19,20,26,30]. To alleviate symptoms in this type of stent, endoscopic balloon dilation[26,30], or argon plasma coagulation have been reported[20], but there are no recommendations to guide what endoscopic approach is best. Other potential complications of BDS that have been addressed are collapse of the biodegradable stent mesh inside the esophageal lumen[21] and tracheoesophageal fistula[31]. Finally, fully covered BDSs could be useful in the treatment of esophageal perforations and anastomotic leaks[32].

Small intestine and colon

BDSs are a promising therapeutic option for benign intestinal and colonic strictures. Strictures following colorectal surgery are the most frequent, and occur in 1.5%-8% of patients[33]. Published information is limited to patients with anastomotic colorectal strictures following resection for colon cancer[34-37], postsurgical colonic fistulas[35], and stricturing Crohn’s disease[38,39] (Table 2). Intestinal insertion is technically possible and relatively simple, except for proximal stenoses and in patients with considerable deformity and angulations. The standard delivery system of PDX-BDS has an active length of 75 cm that limitates proximal stent insertion, and in most cases it may not be possible to place the stent at more than 30 cm from the anus[35]. Technical difficulties for more proximal stenoses are pre-empted due to the necessity of a special introduction system for stent insertion through a balloon overtube[38]. Early stent migration is an important drawback and is the main reason of clinical failure, but can be solved using cyanoacrylate, with a clip placement in the upper flare or by improvements in stent design. Mucosal hyperplasic reaction after insertion of BDS has been documented in esophageal strictures but not in intestinal strictures.

Pancreatobiliary tract

Endoscopic therapy of benign biliary strictures (BBSs) is now first-line therapy. The paper of BDSs in clinical practice is unknown, and is one the main targets in endoscopic research. The causes of BBSs are diverse, with the 2 most common causes being postsurgical strictures and chronic pancreatitis[40]. Commercially available plastic and metal stents for the bile duct and pancreatic duct have many limitations. Endoscopic placement of BDSs have demonstrated feasibility of implantation, relatively safety, and potential efficacy in the biliary and pancreatic ducts in animal models[41,42]. The use of a novel, self-expanding, radiopaque PLA-barium sulphate BDS and a polyethylene stent was investigated in 12 pigs with cystic-duct leakage, showing that the total external output of bile was significantly smaller with BDS compared with the plastic stent group[42]. This group of authors investigated the degradation, patency, and toxicity of this PLA-BDS stent placed into the pancreatic duct of pigs, and after six months no histological or anatomical changes were observed[41].

Recently, other group of authors have developed other self-expandable BDS made from a poliglecaprone, an absorbable surgical suture. This stent was successfully endoscopically inserted in the pancreatic and bile ducts in 4 pigs[43]. However, future animal studies are needed to evaluate the short-term patency, tissue reactivity and degradation of this stent.

There is no published clinical experience with endoscopic placement of BDSs. However, percutaneously placement of BDSs have been addressed recently[44,45]. In this two pilot studies a total of 12 patients with refractory postsurgical BBSs have been treated with BDSs-PDX in the biliary tree, with clinical success with up to 2-years of follow-up.

CONCLUSION

BDSs are an attractive option to avoid ongoing dilation or surgery in patients with benign stenoses of the small and large intestines. The experience with the currently the only BDS for endoscopic placement, made of PDX, have shown promising results. However some aspects should be improved as are the fact that BDSs lose their radial force over time due to the degradable material, and that can cause stent-induced mucosal or parenchymal injury. This complication rate and modest clinical efficacy has to be carefully considered in individual patients prior to placement of BDSs. Otherwise, the price of these stents therefore it is nowadays an important limitation.

REFERENCES

1	Tokar JL, Banerjee S, Barth BA, Desilets DJ, Kaul V, Kethi SR, Pedrosa MC, Pfau PR, Pleskow DK, Varadarajulu S, Wang A, Song LM, Rodriguez SA. Drug-eluting/biodegradable stents. Gastrointest Endosc 2011; 74: 954-958 [PMID: 21944310 DOI: 10.1016/j.gie.2011.07.028]

2	Räber L, Windecker S. Current status of drug-eluting stents. Cardiovasc Ther 2011; 29: 176-189 [PMID: 20370793 DOI: 10.1111/j.1755-5922.2010.00144.x]

3	Freudenberg S, Rewerk S, Kaess M, Weiss C, Dorn-Beinecke A, Post S. Biodegradation of absorbable sutures in body fluids and pH buffers. Eur Surg Res 2004; 36: 376-385 [PMID: 15591748]

4	Gunatillake P, Mayadunne R, Adhikari R. Recent developments in biodegradable synthetic polymers. Biotechnol Annu Rev 2006; 12: 301-347 [PMID: 17045198]

5	Kemppainen E, Talja M, Riihelä M, Pohjonen T, Törmälä P, Alfthan O. A bioresorbable urethral stent. An experimental study. Urol Res 1993; 21: 235-238 [PMID: 8342257]

6	Goldin E, Fiorini A, Ratan Y, Keter D, Loshakove A, Globerman O, Beyar M. A new biodegradable and self-expandable stent for benign esophageal strictures. Gastrointest Endosc 1996; 43: 294 [DOI: 10.1016/S0016-5107(96)80017-4]

7	Fry SW, Fleischer DE. Management of a refractory benign esophageal stricture with a new biodegradable stent. Gastrointest Endosc 1997; 45: 179-182 [PMID: 9041006]

8	Rejchrt S, Kopacova M, Bartova J, Bures J. Intestinal biodegradable stents. initial experience in the czech republic. Folia Gastroenterol Hepatol 2009; 7: 7

9	Canena JM, Liberato MJ, Rio-Tinto RA, Pinto-Marques PM, Romão CM, Coutinho AV, Neves BA, Santos-Silva MF. A comparison of the temporary placement of 3 different self-expanding stents for the treatment of refractory benign esophageal strictures: a prospective multicentre study. BMC Gastroenterol 2012; 12: 70 [PMID: 22691296]

10	Dua KS, Vleggaar FP, Santharam R, Siersema PD. Removable self-expanding plastic esophageal stent as a continuous, non-permanent dilator in treating refractory benign esophageal strictures: a prospective two-center study. Am J Gastroenterol 2008; 103: 2988-2994 [PMID: 18786110 DOI: 10.1111/j.1572-0241.2008.02177.x]

11	Siersema PD. Stenting for benign esophageal strictures. Endoscopy 2009; 41: 363-373 [PMID: 19340743 DOI: 10.1055/s-0029-1214532]

12	Tanaka T, Takahashi M, Nitta N, Furukawa A, Andoh A, Saito Y, Fujiyama Y, Murata K. Newly developed biodegradable stents for benign gastrointestinal tract stenoses: a preliminary clinical trial. Digestion 2006; 74: 199-205 [PMID: 17341853]

13	Saito Y, Tanaka T, Andoh A, Minematsu H, Hata K, Tsujikawa T, Nitta N, Murata K, Fujiyama Y. Usefulness of biodegradable stents constructed of poly-l-lactic acid monofilaments in patients with benign esophageal stenosis. World J Gastroenterol 2007; 13: 3977-3980 [PMID: 17663513]

14	Saito Y, Tanaka T, Andoh A, Minematsu H, Hata K, Tsujikawa T, Nitta N, Murata K, Fujiyama Y. Novel biodegradable stents for benign esophageal strictures following endoscopic submucosal dissection. Dig Dis Sci 2008; 53: 330-333 [PMID: 17713855]

15	Vandenplas Y, Hauser B, Devreker T, Urbain D, Reynaert H. A biodegradable esophageal stent in the treatment of a corrosive esophageal stenosis in a child. J Pediatr Gastroenterol Nutr 2009; 49: 254-257 [PMID: 19561544 DOI: 10.1097/MPG.0b013e31819de871]

16	Orive-Calzada A, Alvarez-Rubio M, Romero-Izquierdo S, Cobo Martin M, Juanmartiñena JF, Ogueta-Fernández M, Molina-Alvarez E, Eraña-Ledesma L. Severe epithelial hyperplasia as a complication of a novel biodegradable stent. Endoscopy 2009; 41 Suppl 2: E137-E138 [PMID: 19544266 DOI: 10.1055/s-0029-1214634]

17	van Hooft JE, van Berge Henegouwen MI, Rauws EA, Bergman JJ, Busch OR, Fockens P. Endoscopic treatment of benign anastomotic esophagogastric strictures with a biodegradable stent. Gastrointest Endosc 2011; 73: 1043-1047 [PMID: 21392754 DOI: 10.1016/j.gie.2011.01.001]

18	Basha J, Appasani S, Vaiphei K, Gupta V, Singh K, Kochhar R. Biodegradable stents: truly biodegradable with good tissue harmony. Endoscopy 2013; 45 Suppl 2 UCTN: E116-E117 [PMID: 23716086 DOI: 10.1055/s-0032-1326111]

19	Fischer A, Bausch D, Baier P, Braun A, Richter-Schrag H. Risk of biodegradable stent-induced hypergranulation causing re-stenosis of a gastric conduit after esophageal resection. Endoscopy 2012; 44 Suppl 2 UCTN: E125-E126 [PMID: 22477178 DOI: 10.1055/s-0031-1291693]

20	Dumoulin FL, Plassmann D. Tissue hyperplasia following placement of a biodegradable stent for a refractory esophageal stricture: treatment with argon plasma coagulation. Endoscopy 2012; 44 Suppl 2 UCTN: E356-E357 [PMID: 23012019]

21	Nogales Rincon O, Huerta Madrigal A, Merino Rodriguez B, Gonzalez Asanza C, Cos Arregui E, Menchen Fernandez-Pacheco P. Esophageal obstruction due to a collapsed biodegradable esophageal stent. Endoscopy 2011; 43 Suppl 2 UCTN: E189-E190 [PMID: 21590596 DOI: 10.1055/s-0030-1256324]

22	Hirdes MM, Siersema PD, van Boeckel PG, Vleggaar FP. Single and sequential biodegradable stent placement for refractory benign esophageal strictures: a prospective follow-up study. Endoscopy 2012; 44: 649-654 [PMID: 22723182 DOI: 10.1055/s-0032-1309818]

23	Dhar A, Topping JH, Johns E, O'Neill D. Biodegradable stents in refractory benign oesophageal strictures -first report of 4 patients from UK. Gastrointest Endosc 2009; 69: AB254 [DOI: 10.1016/j.gie.2009.03.655]

24	Bychkova OV, Lazyuk II, Averin V. Bio-degradable stents - new approach to the treatment of caustic stenoses in children. Folia Gastroenterol Hepatol 2009; 7: 30

25	Martín Cano F, Rodríguez Vargas J, Velasco Sánchez B, Herrera Montes I. Use of self-expandable prosthesis in esophageal stenosis in children. Cir Pediatr 2012; 25: 207-210 [PMID: 23659024]

26	Karakan T, Utku OG, Dorukoz O, Sen I, Colak B, Erdal H, Karatay E, Tahtaci M, Cengiz M. Biodegradable stents for caustic esophageal strictures: a new therapeutic approach. Dis Esophagus 2013; 26: 319-322 [PMID: 22974043 DOI: 10.1111/j.1442-2050.2012.01418.x]

27	Stivaros SM, Williams LR, Senger C, Wilbraham L, Laasch HU. Woven polydioxanone biodegradable stents: a new treatment option for benign and malignant oesophageal strictures. Eur Radiol 2010; 20: 1069-1072 [PMID: 19921200 DOI: 10.1007/s00330-009-1662-5]

28	Griffiths EA, Gregory CJ, Pursnani KG, Ward JB, Stockwell RC. The use of biodegradable (SX-ELLA) oesophageal stents to treat dysphagia due to benign and malignant oesophageal disease. Surg Endosc 2012; 26: 2367-2375 [PMID: 22395954 DOI: 10.1007/s00464-012-2192-9]

29	Repici A, Vleggaar FP, Hassan C, van Boeckel PG, Romeo F, Pagano N, Malesci A, Siersema PD. Efficacy and safety of biodegradable stents for refractory benign esophageal strictures: the BEST (Biodegradable Esophageal Stent) study. Gastrointest Endosc 2010; 72: 927-934 [PMID: 21034894 DOI: 10.1016/j.gie.2010.07.031]

30	Hair CS, Devonshire DA. Severe hyperplastic tissue stenosis of a novel biodegradable esophageal stent and subsequent successful management with high-pressure balloon dilation. Endoscopy 2010; 42 Suppl 2: E132-E133 [PMID: 20405380 DOI: 10.1055/s-0029-1244011]

31	Jung GE, Sauer P, Schaible A. Tracheoesophageal fistula following implantation of a biodegradable stent for a refractory benign esophageal stricture. Endoscopy 2010; 42 Suppl 2: E338-E339 [PMID: 21170838 DOI: 10.1055/s-0030-1256005]

32	Černá M, Köcher M, Válek V, Aujeský R, Neoral Č, Andrašina T, Pánek J, Mahathmakanthi S. Covered biodegradable stent: new therapeutic option for the management of esophageal perforation or anastomotic leak. Cardiovasc Intervent Radiol 2011; 34: 1267-1271 [PMID: 21213108 DOI: 10.1007/s00270-010-0059-9]

33	Luchtefeld MA, Milsom JW, Senagore A, Surrell JA, Mazier WP. Colorectal anastomotic stenosis. Results of a survey of the ASCRS membership. Dis Colon Rectum 1989; 32: 733-736 [PMID: 2667922]

34	Repici A, Pagano N, Rando G, Carlino A, Vitetta E, Ferrara E, Strangio G, Zullo A, Hassan C. A retrospective analysis of early and late outcome of biodegradable stent placement in the management of refractory anastomotic colorectal strictures. Surg Endosc 2013; 27: 2487-2491 [PMID: 23443478 DOI: 10.1007/s00464-012-2762-x]

35	Pérez Roldán F, González Carro P, Villafáñez García MC, Aoufi Rabih S, Legaz Huidobro ML, Sánchez-Manjavacas Múñoz N, Roncero García-Escribano O, Ynfante Ferrús M, Bernardos Martín E, Ruiz Carrillo F. Usefulness of biodegradable polydioxanone stents in the treatment of postsurgical colorectal strictures and fistulas. Endoscopy 2012; 44: 297-300 [PMID: 22261748 DOI: 10.1055/s-0031-1291482]

36	Toth E, Nielsen J, Nemeth A, Wurm Johansson G, Syk I, Mangell P, Almqvist P, Thorlacius H. Treatment of a benign colorectal anastomotic stricture with a biodegradable stent. Endoscopy 2011; 43 Suppl 2 UCTN: E252-E253 [PMID: 21837599 DOI: 10.1055/s-0030-1256511]

37	Janík V, Horák L, Hnaníček J, Málek J, Laasch HU. Biodegradable polydioxanone stents: a new option for therapy-resistant anastomotic strictures of the colon. Eur Radiol 2011; 21: 1956-1961 [PMID: 21533633 DOI: 10.1007/s00330-011-2131-5]

38	Rejchrt S, Kopacova M, Brozik J, Bures J. Biodegradable stents for the treatment of benign stenoses of the small and large intestines. Endoscopy 2011; 43: 911-917 [PMID: 21623562 DOI: 10.1055/s-0030-1256405]

39	Rodrigues C, Oliveira A, Santos L, Pires E, Deus J. Biodegradable stent for the treatment of a colonic stricture in Crohn’s disease. World J Gastrointest Endosc 2013; 5: 265-269 [PMID: 23678382 DOI: 10.4253/wjge.v5.i5.265]

40	Kaffes AJ, Liu K. Fully covered self-expandable metal stents for treatment of benign biliary strictures. Gastrointest Endosc 2013; 78: 13-21 [PMID: 23548962 DOI: 10.1016/j.gie.2013.02.019]

41	Laukkarinen J, Lämsä T, Nordback I, Mikkonen J, Sand J. A novel biodegradable pancreatic stent for human pancreatic applications: a preclinical safety study in a large animal model. Gastrointest Endosc 2008; 67: 1106-1112 [PMID: 18291398 DOI: 10.1016/j.gie.2007.10.013]

42	Laukkarinen J, Nordback I, Mikkonen J, Kärkkäinen P, Sand J. A novel biodegradable biliary stent in the endoscopic treatment of cystic-duct leakage after cholecystectomy. Gastrointest Endosc 2007; 65: 1063-1068 [PMID: 17531643]

43	Itoi T, Kasuya K, Abe Y, Isayama H. Endoscopic placement of a new short-term biodegradable pancreatic and biliary stent in an animal model: a preliminary feasibility study (with videos). J Hepatobiliary Pancreat Sci 2011; 18: 463-467 [PMID: 21170555 DOI: 10.1007/s00534-010-0364-3]

44	Mauri G, Michelozzi C, Melchiorre F, Poretti D, Tramarin M, Pedicini V, Solbiati L, Cornalba G, Sconfienza LM. Biodegradable biliary stent implantation in the treatment of benign bilioplastic-refractory biliary strictures: preliminary experience. Eur Radiol 2013; 23: 3304-3310 [PMID: 23842947]

45	Petrtýl J, Brůha R, Horák L, Zádorová Z, Dosedel J, Laasch HU. Management of benign intrahepatic bile duct strictures: initial experience with polydioxanone biodegradable stents. Endoscopy 2010; 42 Suppl 2: E89-E90 [PMID: 20195981 DOI: 10.1055/s-0029-1243880]

P- Reviewers: Mudawi HMY, Loras C, Pan WS    S- Editor: Zhai HH    L- Editor: A    E- Editor: Liu XM

# Text boxes

Table 2  Cases series evaluating the outcomes of biodegradable stents with polydioxanone for benign intestinal and colonic strictures

| Ref. | Year | Type of study | Indication | n | Follow-up (mo) | Technical success | Complications | Clinical success |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Janík et al[37] | 2011 | CS | PS | 3 | 5 | 100% | 0% | 66% |
| Rejchrt et al[8] | 2009 | CS | Stricturing CD | 11 | 14 | 91% | Stent migration, 27% | 64% |
| Toth et al[36] | 2011 | CR | PS | 1 | 5 | 100% | 0% | 100% |
| Pérez Roldán et al[35] | 2012 | CS | PS and fistula | 10 | 13 | 90% | Stent migration, 10% | 50% |
| Repici et al[34] | 2013 | CS | PS | 11 | 3 | 100% | Stent migration, 36% | 45% |
| Rodrigues et al[39] | 2013 | CR | Stricturing CD | 1 | 16 | 100% | 0% | 100% |

CR: Case report; CS: Case series; RCT: Randomized clinical trial; CD: Crohn’s disease; PS: Postsurgical strictures.

Table 1  Cases series evaluating the outcomes of biodegradable stents with polydioxanone for refractory benign esophageal strictures

| Ref. | Year | Type of study | n | Follow-up (mo) | Technical success | Complications | Clinical success |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Dhar et al[23] | 2009 | CS | 4 | 4 | 100% | Chest pain, 25% | 50% |
| Vandenplas et al[15] | 2009 | CR | 1 | 4 | 100% | 0% | 100% |
| Orive-Calzada et al[16] | 2009 | CR | 1 | 3 | 100% | T. hyperplasia, 100% | 0% |
| Stivaros et al[27] | 2010 | CS | 2 | 7 | 100% | Chest pain, 50% | 50% |
|  |  |  |  |  |  | Stent migration, 50% |  |
| Bychkova et al[24] | 2009 | CR | 1 | 4 | 100% | 0% | 100% |
| Hair et al[30] | 2010 | CR | 1 | 8 | 100% | T. hyperplasia, 100% | 0% |
| van Hooft et al[17] | 2011 | CS | 10 | 6 | 100% | Chest pain, 20% | 60% |
| Repici et al[29] | 2010 | CS | 21 | 13.2 | 100% | Chest pain, 14% | 45% |
|  |  |  |  |  |  | Hemorrhage, 5% |  |
|  |  |  |  |  |  | Stent migration, 9% |  |
| Nogales Rincon et al[21] | 2011 | CR | 1 | 2 | 100% | Stent collapse, 100% | 0% |
| Martín Cano et al[25] | 2012 | CS | 3 | 4 | 100% | 0% | 100% |
| Griffiths et al[28] | 2012 | CS | 7 | 4 | 96% | 0% | 76% |
| Canena et al[9] | 2012 | RCT | 10 | 12 | 100% | Chest pain, 10% | 30% |
|  |  |  |  |  |  | Hemorrhage, 10% |  |
|  |  |  |  |  |  | Stent migration, 20 |  |
|  |  |  |  |  |  | T. hyperplasia, 30% |  |
| Fischer et al[19] | 2012 | CS | 2 | 12 | 100% | T. hyperplasia, 50% | 50% |
| Dumoulin et al[20] | 2012 | CR | 1 | 18 | 100% | T. hyperplasia, 100% | 0% |
| Hirdes et al[22] | 2012 | CS | 28 | 10 | 100% | Chest pain, 22% | 25% |
|  |  |  |  |  |  | Hemorrhage, 8% |  |
| Basha et al[18] | 2013 | CR | 1 | 4 | 100% | 0% | 0% |
| Karakan et al[26] | 2013 | CS | 7 | 15 | 100% | T. hyperplasia, 57% | 43% |

CR: Case report; CS: Case series; RCT: Randomized clinical trial; T. hyperplasia: Tissue hyperplasia.