Name of journal: World Journal of Gastroenterology

ESPS Manuscript NO: 7757

Columns: BRIEF ARTICLE

Evaluation of a novel choanoid fluidized bed bioreactor for future bioartificial liver

Yu CB et al. Evaluation of choanoid fluidized bed bioreactor

Cheng-Bo Yu, Xiao-Ping Pan, Liang Yu, Xiao-Peng Yu, Wei-Bo Du, Hong-Cui Cao, Jun Li, Ping Chen, Lan-Juan Li

Cheng-Bo Yu, Xiao-Ping Pan, Liang Yu, Xiao-Peng Yu, Wei-Bo Du, Hong-Cui Cao, Jun Li, Ping Chen, Lan-Juan Li, States Key Laboratory for Diagnosis and Treatment of Infectious, Diseases，the First Affiliated Hospital, School of Medicine, Zhejiang University, Hangzhou 310003, Zhejiang Province, China

Xiao-Ping Pan, Wei-Bo Du, Hong-Cui Cao Jun Li, Lan-Juan Li, Collaborative Innovation Center for Diagnosis and Treatment of Infectious Diseases, Hangzhou 310003, Zhejiang Province, China

Author contributions: Yu CB wrote the paper; Pan XP, Yu L, Yu XP, Du WB, Cao HC, Li J, Chen P critically reviewed the manuscript for important intellectual content; Li LJ supervised the study; all authors have read and approved the final manuscript to be published.

Supported by The Grants from the National Scientific and Technological Major Project of China, Grant No. 2011ZX10004-901, No. 2013ZX10004904; the National Science and Technology Major Project, No. 2012ZX10002006

Correspondence to: Lan-Juan Li, MD, State Key Laboratory for Diagnosis and Treatment of Infectious Disease, First Affiliated Hospital, Zhejiang University School of Medicine, 79 Qingchun Road, Hangzhou 310003, Zhejiang Province, China. ljli@zju.edu.cn

Telephone: +86-571-87236458     Fax: +86-571-87236459

Received: November 29, 2013     Revised: February 26, 2014

Accepted: March 6, 2014

Published online:

Abstract

AIM: To construct and evaluate the functionality of a choanoid-fluidized bed bioreactor (CFBB) based on microencapsulated immortalized human hepatocytes.

METHODS: Encapsulated hepatocytes were placed in the constructed CFBB and circulated through Dulbecco’s Modified Eagle’s Medium (DMEM) for 12 h, and then through exchanged plasma for 6 h, and compared with encapsulated cells cultivated under static conditions in a spinner flask. Levels of alanine aminotransferase (ALT) and albumin were used to evaluate the CFBB during media circulation, whereas levels of ALT, total bilirubin (TBil), and albumin were used to evaluate it during plasma circulation. Mass transfer and hepatocyte injury were evaluated by comparing the results from the two experimental conditions. In addition, the viability and microstructure of encapsulated cells were observed in different environments.

RESULTS: The bioartificial liver model based on a CFBB was verified by in vitro experiments. The viability of encapsulated cells accounting for 84.6% ± 3.7% in CFBB plasma perfusion was higher than the 74.8% ± 3.1% in the static culture group (P < 0.05) after 6 h. ALT release from cells was 29 ± 3.5 U/L vs 40.6 ± 3.2 U/L at 12 h (P < 0.01) in the CFBB medium circulation and static medium culture groups, respectively. Albumin secretion from cells was 234.2 ± 27.8 g/1 × 107 cells vs 167.8 ± 29.3 g/1 × 107 cells at 6 h (P < 0.01), 274.4 ± 34.6 g/1 × 107 cells vs 208.4 ± 49.3 g/1 × 107 cells (P < 0.05) at 12 h in the two medium circulation/culture groups, respectively. Furthermore, ALT and TBil levels were 172.3 ± 24.1 U/L vs 236.3 ± 21.5 U/L (P < 0.05), 240.1 ± 23.9 mol/L vs 241.9 ± 31.4 mol/L (P > 0.05) at 6 h in the CFBB plasma perfusion and static plasma culture groups, respectively. There was no significant difference in albumin concentration between the two experimental plasma groups at any time point. The microstructure of encapsulated hepatocytes remained healthier in the CFBB group compared with the static culture group after 6 h plasma perfusion.

CONCLUSION: The CFBB can function as a bioartificial liver based on a bioreactor. The efficacy of this novel bioreactor is promising for the study of liver failure.

© 2014 Baishideng Publishing Group Co., Limited. All rights reserved.

Key words: Choanoid; Fluidized bed; Bioreactor; Immortalized human hepatocytes; Bioartificial liver

Core tip: We newly constructed a choanoid fluidized bed bioreactor (CFBB) and received a national invention patent. We evaluated the CFBB functionality based on microencapsulated immortalized human hepatocytes. For this purpose, we placed the cultured hepatocytes into the CFBB and circulated through Dulbecco’s Modified Eagle’s Medium media for 12 h and through exchanged plasma for 6 h. The bioartificial liver based on a fluidized-bed bioreactor with microencapsulated immortalized human hepatocytes appeared to be effective for improving severe hepatitis plasma parameters. The efficacy of this novel bioreactor is promising for the study of liver failure.

Yu CB, Pan XP, Yu L, Yu XP, Du WB, Cao HC, Li J, Chen P, Li LJ. Evaluation of a novel choanoid fluidized bed bioreactor for future bioartificial liver.

Available from: URL:

DOI:

INTRODUCTION

Despite recent considerable improvements in supportive therapy, fulminant hepatic failure has a high mortality worldwide[1]. To date, the only effective long-term treatment is orthotropic liver transplantation. However, there is a worldwide shortage of organ donors. A bioartificial liver (BAL) support system is expected to be a new tool for end-stage liver failure after injury or for bridge-to-transplantation use[2,3]. Researchers have developed extracorporeal BALs to investigate the potential performance of hepatocytes immobilized in a bioreactor. Such devices should be able to replace all or most liver functions[4, 5].

Presently, various configurations of BALs have been proposed using flat plate and monolayer bioreactors[6,7], hollow fiber[8,9], perfused beds or scaffolds[10-12], beds with encapsulated or suspended cells[13,14], and other complicated configurations with compound bioreactors[15]. The most widely investigated bioreactor at present is based on a hollow fiber membrane. However, this model is difficult to scale up. Moreover, the semipermeable membrane can act as a diffusion barrier between the hepatocytes and the plasma of patients; therefore, the xenogenic hepatocytes are placed directly in contact with patient plasma without an impermeable immunological barrier. As such, hepatocytes immobilized into alginate/chitosan (AC) microcapsules might be an interesting alternative.

Encapsulated cells hosted in bioreactors may enhance mammalian cell culture within a controlled and efficient environment[16]. At present, AC has been widely applied for immobilization or encapsulation of biological constituents due to its stability, compatibility, and simplicity of use[17]. This immobilization allows growth of hepatocytes in a favorable environment because the porous structure of AC maintains a close interaction with the external medium. Exchange between beads and medium can be achieved in flasks or bioreactors. Within a bioreactor, the microcapsules are usually hosted either in a fixed or fluidized bed. In a fixed bed, the beads cannot withstand the extreme stresses caused by high perfusion velocity. The fluid often mobilizes through channels in the space that is devoid of beads, which results in formation of a void volume or dead space in the traditional fluidized bed bioreactors. We developed a BAL based on a choanoid-fluidized bed bioreactor (CFBB) configuration that allowed the fluidization of AC beads in which cells can be immobilized. In terms of liver support, substances such as albumin and other macromolecules should be exchanged between the ambient media (the patient’s plasma) and the encapsulated cells. Mass transfer occurs in both directions: from the surrounding fluid into the beads (oxygen, nutrients, or substances to be metabolized by hepatocytes), and from the beads into the surrounding fluid (substances secreted by the cells).

In order to confirm functionality of the CFBB, it is important to demonstrate stable function of the encapsulated immortalized human hepatocyte line during perfusion in culture medium or potentially toxic liver failure (LF) plasma. So far, only a few groups have attempted to assess its effects on cells grown in 3D cultures in the context of a BAL[18,19]. Other studies that assess functionality of 3D hepatocyte cultures in putative BALs have perfused their systems with culture medium[20]. In this study, we evaluated the newly constructed bioreactor using AC microcapsules that contain the immortalized HepLi4 human hepatocyte line established in our laboratory.

MATERIALS AND METHODS

CFBB

The CFBB consists of a column containing AC beads. The column size was 500 mL, which was designed for a perfusion plasma flow rate ranging from 80 to 120 mL/min and a bead volume of 400 mL. The bioreactor height allowed for a safety volume theoretically free of beads at the top of the column. The materials used for the cylinders were biocompatible. The different components are shown in Figure 1 and are labeled for reference. The microcapsule access port enabled ease of filling of microencapsulated hepatocytes, while the blood sample port allowed fluid samples to be taken during the operation. In addition, the cell sieve prevented cells or cell debris from being released into the fluid circulation. The total length of the CFBB was 250 mm. This bioreactor device has received a national invention patent (patent number: ZL200710070279.0).

Immortalization of human hepatocytes

The immortalization of HepLi4 was established from a brain-dead male by transfection with pcDNA 3.1 (–) recombinant plasmid containing the genes encoding SV40 LT antigen.

Hepatocyte isolation and microencapsulation preparation

The hepatocytes were cultured for 4 d, isolated, and then suspended in 1.8% high-viscosity sodium alginate solution (Sigma, St Louis, MO, United States). The concentration of hepatocytes in the final solution was 2 × 106 viable cells/mL. Droplets of cell solution formed by a drop generator fell into a 0.6% (w/v) chitosan solution, and the size of droplets ranged from 500 to 600 mm. The microencapsulation procedure has been previously described[21]. After culturing in special spinners for 2 wk, the function of the microencapsulated hepatocytes was been shown to be at a maximum[22]. Viable hepatocytes (5 × 109 cells) were loaded into the CFBB.

Preparation of CFBB

The CFBB was treated with hypochlorite solution, ethanol, and 0.02% collagen solution (Nichirei, Tokyo, Japan). Dulbecco’s Modified Eagle’s Medium (DMEM) was passed through the circuit for 2 h prior to the experiment. Microencapsulated hepatocytes (5 × 109), which had viability consistently > 90%, were loaded into the CFBB. A CFBB containing AC microcapsules encapsulating viable hepatocytes was inserted in the flow circuit containing a medium reservoir and peristaltic pump.

Study groups

Group 1 (Control group): AC microcapsules hosting cells in static medium/plasma (n = 5 tests). Group 2 (Experiment group): AC microcapsules hosting cells in the fluidized bed bioreactor (n = 5 tests)

Extracorporeal culture medium perfusion

Culture medium was introduced at the bottom of the bioreactor. For the in vitro experiment, a 1500-mL reservoir was installed between the peristaltic pump and BAL module. Oxygen was supplied by bring the culture medium into contact with a gas mixture of 95% O2 and 5% CO2, using silastic tubing. The optimal flow rate of fluid for proper fluidization of entrapped hepatocytes was 100 mL/min, and the temperature was maintained at 37 °C (Figure 2).

Determination of BAL medium perfusion system in vitro

Cell viability: Cell viability was assessed by trypan blue exclusion before and after medium perfusion. The count was performed with a hemocytometer as hepatocytes were detached after AC dissolution in citrate buffer (pH 7.4).

Function of the BAL medium perfusion system: Independent experiments were performed five times with the BAL device. Samples of microencapsulated hepatocytes in DMEM were obtained at 2-h intervals during 12 h circulation. Changes in alanine aminotransferase (ALT) and albumin levels were determined with an automatic biochemical analyzer (Hitachi 7600, Tokyo, Japan).

Exchanged plasma perfusion in vitro: The exchanged plasma, collected from patients with severe hepatitis, was diluted twice with physiological saline, which was set up at the bottom of the bioreactor, as described above, for the in vitro experiments (Figure 2). The optimal flow rate of fluid for proper fluidization of entrapped hepatocytes was 85 mL/min, and the temperature was maintained at 37°C.

Determination of the BAL plasma perfusion system in vitro

Cell viability: The cell viability was assessed by trypan blue exclusion before and after plasma perfusion, as described above.

Function of the BAL plasma perfusion system: Independent experiments were performed five times with the BAL device. Plasma samples were obtained before and after circulation. Changes in ALT, total bilirubin (TBil) and albumin levels were determined.

Transmission electron microscopy: Microencapsulated hepatocytes in the fluidized bed and static culture groups obtained before and after circulation were observed by transmission electron microscopy (TEM) (JEM-1200EXII; Jeol). Specimens were fixed in 2.5% glutaraldehyde (pH 7.4) overnight at 4°C, followed by post-fixation in 1% osmium tetroxide for 1 h and by progressive dehydration in an ethanol series (50–100%, v/v), and then finally embedded in Epon (Hexion Specialty Chemicals, Columbus, OH, USA), followed by pathologic serial thin section cutting Thin sections were observed and photographed with an electron microscope (JEM-1200EXII; Jeol). The specimens were examined by TEM after plating with gold under vacuum. Areas for examination were randomly chosen.

Statistical analysis

Measurements are presented as mean ±SD and comparisons were made using Student’s t test. In univariate analyses significance was accepted at P ≤ 0.05. SPSS for Windows Version 16.0 (Chicago, IL, United States) was used for data analysis.

RESULTS

Cell viability

The viability of encapsulated cells in the CFBB group was 93.5 ± 3.2% at the beginning of the experiment and 90.6% ± 6.5% after 12 h (P > 0.05). The viability of encapsulated hepatocytes in the static culture flask decreased from 93.9% ± 4.4% to 86.8% ± 3.8% after 12 h (P > 0.05).

Function of the BAL medium perfusion system

ALT levels: As shown in Figure 3, ALT was released from beads containing hepatocytes maintained under static culture conditions and culture medium in the CTBB. In the fluidized bioreactor group, the ALT release was 16.4 ± 2.7 U/L after 2 h, which increased to 29 ± 3.5 U/L after 12 h. ALT released from the cells in the static culture group was 19 ± 2.7 U/L at 2 h and 40.6 ± 3.2 U/L at 12 h. These data indicate that ALT release from the fluidized bioreactor was significantly lower compared with that from the static medium culture group from 4 to 12 h (4 h, 12 h, P < 0.01; 6 h, P < 0.05).

Albumin secretion: As indicated in Figure 4, the amount of albumin secreted after 2 h (94.4 ± 11.1 g/1 × 107 cells) was significantly increased by 6 h in the cells within the CFBB (234.2 ± 27.8 g/1 × 107 cells) (P < 0.01), which was further increased to 274.4 ± 34.6 g/1 × 107 cells (P < 0.01) after 12 h. The amount of albumin secreted from cells in the static culture group was 94.6 ± 19.8 g/1 × 107 cells, 167.8 ± 29.3 g/1 × 107 cells, and 208.4 ± 49.3 g/ 1 × 107 cells at 2 h, 6 h, and 12 h, respectively. Albumin secretion form cells in the CFBB group was significantly higher than from cells in the static culture group after 6–12 h (6 h, P < 0.01; 12 h, P < 0.05).

Determination of the BAL plasma perfusion system in vitro

Cell viability: The viability of encapsulated cells in the fluidized bed plasma perfusion group was 94.5% ± 3.2% at the beginning of the experiment, which decreased to 84.6% ± 3.7% after 6 h (P < 0.05). The viability of encapsulated hepatocytes in the static culture flask decreased from 95.2% ± 4.4% at the beginning of the experiment to 74.8% ± 3.1% after 6 h (P < 0.01). The two groups were significantly different after 6 h (P < 0.05).

Function of the BAL plasma perfusion system

ALT levels: As shown in Figure 5, ALT levels before and after plasma perfusion through the fluidized bed were increased after 6 h (from 141.7 ± 31.9 U/L to 172.3 ± 24.1 U/L, P < 0.05). There was a significant increase in ALT levels in the plasma of the static culture group after 6 h (139 ± 37.6 to 236.3 ± 21.5 U/L, P < 0.01). The level of ALT after the experiment in the static plasma culture group was significantly higher than that in the plasma in the fluidized bed group (P < 0.05).

TBil concentration: As shown in Figure 6, the concentration of TBil before and after plasma perfusion through the fluidized bed was decreased (228.7 ± 24.3 mol/L to 240.1 ± 23.9 mol/L, P > 0.05), while the concentration in the plasma before and after static culture showed no significant change (226.6 ± 27.8 mol/L to 241.9 ± 31.4 mol/L, P > 0.05). The TBil concentration in the plasma perfusion group after the experiment was not significantly different compared with that in the static plasma culture group (P > 0.05).

ALB concentration: As shown in Figure 7, there was no significant difference in albumin concentration between the two experimental groups at any time point.

TEM

Before the experiments, encapsulated hepatocytes were maintained in a healthy growth state with cohesive colonies. TEM showed normal hepatocyte subcellular architecture with mitochondria, endoplasmic reticulum, nuclei with prominent nucleoli, lipid vacuoles, and pools of glycogen. In addition, desmosomes, hemidesmosomes, bile canaliculi-like formation, and junction complexes were well formed, and there was striking formation of canaliculi lined with microvilli (Figure 8). After the experiments, encapsulated hepatocytes in the CFBB group still possessed numerous mitochondria, endoplasmic reticulum, desmosomes, bile canaliculi-like formation, and junction complexes, with only a small amount of vacuolization (Figure 9). However, some cells in the static plasma culture group had shrunken nuclei and some cells showed vacuolar degeneration, although there were cells with many organelles, mitochondria, microvilli, and tight junctions (Figure 10).

DISCUSSION

Day 14 was determined to be the optimal time to use the cells for the CFBB devices, which were constructed by scaling up and evaluating the encapsulated immortalized human hepatocyte cells with spinner cultivation (data not shown). The work described here will provide an important foundation to evaluate the bioreactor for potential use as a BAL in the future. We also investigated the structural parameters of the bioreactor, which played a key role in providing beneficial technical support for the bioreactor assessment. Using the CFBB, we investigated the effect of fluidization on the metabolism of the encapsulated hepatocytes by circulating culture medium for 6–12 h, and to verify whether this bioreactor could replace part of the normal liver and serve as an extracorporeal BAL.

For the objective and comprehensive study of the bioreactor, we studied medium circulation and the exchange of plasma isolated from patients with severe hepatitis while circulating it through the CFBB. The bioactive component was in the encapsulated immortalized human hepatocytes, which was circulated in the CFBB. For the control group, the beads containing hepatocytes were maintained in a spinner culture flask under static conditions. For the CFBB group, the beads containing hepatocytes were circulated in the fluidized bed. The hepatocytes (5 × 109) were placed in the CFBB, and DMEM with high glucose concentration was circulated through the bioreactor for 12 h to determine the effect of fluidization on hepatocyte metabolism. The exchanged plasma was perfused in vitro for 6 h to determine the effect of encapsulated hepatocytes on the metabolism of plasma from patients with severe hepatitis, and the toxic effect of this plasma on the encapsulated hepatocytes in the CFBB. We determined whether hepatocytes could function properly in the fluidization state compared with those in the static culture conditions, in the presence of plasma isolated from patients with severe hepatitis. Perfusion was conducted for 6–12 h, which is the length of plasma exchange in combination with continuous renal replacement therapies session. It is generally recognized that the extracorporeal circulation should be interrupted after this time period and that several consecutive sessions, using several bioreactors, should be performed before transplantation[23,24]. Therefore, we did not study the long-term metabolism of encapsulated hepatocytes because the application of the bioreactor is not recommended as a long-term culture device.

In vitro media circulation is easier to perform, therefore, we compared the function of the encapsulated hepatocytes under fluidized versus static culture conditions. The index of encapsulated hepatocyte injury, such as the release of ALT, was significantly lower in the fluidized bed group because microcapsules provided a 3D growth environment, and the fluidization state of the encapsulated hepatocytes in the CFBB promoted more rapid bidirectional mass exchange. In contrast, diffusion of metabolites from encapsulated hepatocytes was slower out of the microcapsules in the static culture group, which could lead to accumulation of metabolites and perhaps damage to the hepatocytes. Furthermore, the hepatocytes in the static culture lacked effective nutrition because they clustered together. Therefore, the level of ALT was increased in the static culture group, while there was no significant increase observed in the CFBB group. This indicated increased mass exchange due to the fluidization and diffusion through the myriad of micropores in the microcapsules. Similarly, the level of albumin released from hepatocytes in the CFBB group was higher compared with that in the static culture group. These data indicate that fluidization in the CFBB could improve the function and viability of encapsulated hepatocytes.

To evaluate the CFBB better, the exchanged plasma from patients with severe hepatitis was used to simulate patient treatment, which was used to complement the animal experiments. The plasma circulated through the CFBB had 5 × 109 cells, which met the preliminary requirements of the BAL. In addition, we studied the effect of encapsulated hepatocytes under fluidization conditions on exchanged plasma from patients with severe hepatitis. We have previously tried to use the concentrated “toxic” plasma (not diluted) in our research model. However, after the 6-h BAL session, SEM data indicated that the hepatocytes were necrotic and cell viability was markedly decreased (data not shown). This might be related to the toxic effect induced by the high toxin levels present in the plasma of patients with severe hepatitis. Therefore, we diluted the concentrated plasma twofold for these experiments. The measured parameters were related to the structural integrity of the hepatocytes, including their viability, because ALT is a cytoplasmic enzyme that is released after damage to the hepatocytes. In addition, the metabolic and synthetic functions of hepatocytes were indicated by the TBil and albumin measurements. In this study, a statistical significance such as the cell viability and ALT level in both groups was observed after the 6-h BAL session, which indicated decreased damage to the hepatocytes in the CFBB group. The plasma levels of enzymes and albumin in the CFBB group that contained encapsulated hepatocytes were likely due to the protective effect of fluidization compared to the static conditions. Moreover, the TBil concentration was slightly increased after plasma circulation because of the lack of bilirubin excretion mechanism in our system, which suggests that an absorber of bilirubin is necessary in BAL circulation.

The ultrastructure of microencapsulated hepatocytes was also observed after the plasma experiments. We found that the hepatocytes remained viable and many organelles were healthy, with only slight necrosis in the CFBB group. In contrast, after 6 h of static culture, the encapsulated hepatocytes presented with obvious necrosis and vacuolization. Therefore, we conclude that the CFBB bioreactor system can maintain functional hepatocytes that are protected from potential toxins.

This study was only performed in vitro; we did not use a BAL in vivo in our study. Therefore, these factors must be considered in a large-animal model of severe liver failure or preclinical application in future research. By creating a hybrid of the CFBB with a BAL, more toxic elements would be removed, and thus longer-lasting effects could be exerted by the BAL, which will be investigated in the future.

The technology described in this experiment is simple to operate, although the systematic evaluation has yet to be demonstrated. Previously, the curative effect of BALs has generally been observed through animal liver failure induced by drug poisoning and small liver remnant volume or anhepatic state postoperatively[25-27]. Currently, there are no systematic data describing the exchange plasma of patients with severe hepatitis as an alternative to animal models for the curative effect of BAL. The merits of this method are as follows: (1) a rich source of plasma with aseptic collection; (2) this technique precludes the effect of multiple factors on the curative effect of BAL, which is favorable for the BAL mechanism; (3) the plasma was isolated from patients with severe hepatitis, therefore, the surrogate model meets the clinical requirements of severe hepatitis with more practical significance; and (4) it is a low-cost method with good repeatability, and it is easy to operate. Inevitably, some limitations exist. This technique has only been conducted in vitro, thus, it may not be extrapolated to animal or human studies because there are differences between the two systems. Therefore, these considerations should be addressed in the future. The CFBB can function as a bioartificial liver based on a bioreactor. The efficacy of this novel bioreactor is promising for the study of liver failure.

COMMENTS

Background

A bioartificial liver (BAL) support system is expected to be a new tool for terminal-stage liver failure. Bioreactor is the key device for BAL system. The most widely investigated bioreactor at present is based on a hollow fiber membrane. However, this model is difficult to scale up. Moreover, the semi-permeable membrane can act as a diffusion barrier between the hepatocytes and the plasma of patients; therefore, the xenogenic hepatocytes are placed directly in contact with patient plasma without an impermeable immunological barrier. As such, hepatocytes immobilized into alginate/chitosan (AC) microcapsules might be an interesting alternative. Within a bioreactor, the microcapsules are usually hosted either in a fixed or fluidized bed. In a fixed fluidized bed, the beads cannot withstand the extreme stresses caused by high perfusion velocity. The fluid often mobilizes through channels in the space that is devoid of beads, which results in formation of a void volume or dead space in the traditional fluidized bed bioreactors.

Research frontiers

Fluidized bed bioreactor is fit for encapsulated hepatocytes. In the area of fixed fluidized bed bioreactor, the beads cannot withstand the extreme stresses caused by high perfusion velocity and the BAL based on fixed fluidized bed has inefficiency of mass exchange, so the research hotspot is how to overcome the extreme stress and decrease the void volume or dead space in the traditional fluidized bed bioreactors.

Innovations and breakthroughs

In this study, the authors newly constructed a choanoid fluidized bed bioreactor (CFBB) and received a national invention patent. Traditional fluidized bed bioreactors have some shortcomings such as a void volume or dead space, which directly affect the stability and mass exchange of the BAL. To address these problems, the authors constructed this bioreactor which is characterized by a perfect combination of the “choanoid” form and fluidized bed. The BAL based on a CFBB with microencapsulated immortalized human hepatocytes appeared to be effective in treatment of severe hepatitis plasma associated with protection of hepatocytes. The efficacy of this novel bioreactor seemed to be promising for the study of liver failure.

Applications

The study results suggest that the CFBB is a potential BAL key device that could be promising for the study of liver failure.

Terminology

Bioreactors, as a key device in bioartificial liver system, can provide a favorable growth and metabolic environment, mass exchange, and immunological isolation as a platform. Fluidized bed is formed when a quantity of a solid is placed under appropriate conditions to cause the solid/fluid mixture to behave as a fluid. This is usually achieved by the introduction of pressurized fluid through the particulate medium. The resulting phenomenon is called fluidization. Fluidized beds are used for several purposes, such as fluidized bed reactors (types of chemical reactors), or mass transfer.

Peer review

This is a good descriptive study in which the authors constructed and evaluate a novel choanoid fluidized bed bioreactor based on extracorporeal circulation. The results are interesting and suggest that the CFBB can function as a bioartificial liver based on a bioreactor and the efficacy of this novel bioreactor is promising for the study of liver failure.

REFERENCES

1 Lee WM, Squires RH, Nyberg SL, Doo E, Hoofnagle JH. Acute liver failure: Summary of a workshop. Hepatology 2008; 47: 1401-1415 [PMID: 18318440 DOI: 10.1002/hep.22177]

2 Frühauf NR, Oldhafer KJ, Höltje M, Kaiser GM, Frühauf JH, Stavrou GA, Bader A, Broelsch CE. A bioartificial liver support system using primary hepatocytes: a preclinical study in a new porcine hepatectomy model. Surgery 2004; 136: 47-56 [PMID: 15232539 DOI: 10.1016/j.surg.2003.12.017]

3 Tilles AW, Berthiaume F, Yarmush ML, Toner M. Critical issues in bioartificial liver development. Technol Health Care 2002; 10: 177-186 [PMID: 12118141]

4 Gerlach JC. Development of a hybrid liver support system: a review. Int J Artif Organs 1996; 19: 645-654 [PMID: 8970832]

5 Tilles AW, Berthiaume F, Yarmush ML, Tompkins RG, Toner M. Bioengineering of liver assist devices. J Hepatobiliary Pancreat Surg 2002; 9: 686-696 [PMID: 12658402 DOI: 10.1007/s005340200095]

6 Shito M, Kim NH, Baskaran H, Tilles AW, Tompkins RG, Yarmush ML, Toner M. In vitro and in vivo evaluation of albumin synthesis rate of porcine hepatocytes in a flat-plate bioreactor. Artif Organs 2001; 25: 571-578 [PMID: 11493279 DOI: 10.1046/j.1525-1594.2001.025007571.x]

7 Shito M, Tilles AW, Tompkins RG, Yarmush ML, Toner M. Efficacy of an extracorporeal flat-plate bioartificial liver in treating fulminant hepatic failure. J Surg Res 2003; 111: 53-62 [PMID: 12842448 DOI: 10.1016/S0022-4804(03)00048-9]

8 Lu HF, Lim WS, Zhang PC, Chia SM, Yu H, Mao HQ, Leong KW. Galactosylated poly(vinylidene difluoride) hollow fiber bioreactor for hepatocyte culture. Tissue Eng 2005; 11: 1667-1677 [PMID: 16411812 DOI: 10.1089/ten.2005.11.1667]

9 Ho Ye S, Watanabe J, Takai M, Iwasaki Y, Ishihara K. High functional hollow fiber membrane modified with phospholipid polymers for a liver assist bioreactor. Biomaterials 2006; 27: 1955-1962 [PMID: 16239028 DOI: 10.1016/j.biomaterials.2005.09.041]

10 Wen F, Chang S, Toh YC, Arooz T, Zhuo L, Teoh SH, Yu H. Development of dual-compartment perfusion bioreactor for serial coculture of hepatocytes and stellate cells in poly(lactic-co-glycolic acid)-collagen scaffolds. J Biomed Mater Res B Appl Biomater 2008; 87: 154-162 [PMID: 18431752 DOI: 10.1002/jbm.b]

11 Chen JP, Lin CT. Dynamic seeding and perfusion culture of hepatocytes with galactosylated vegetable sponge in packed-bed bioreactor. J Biosci Bioeng 2006; 102: 41-45 [PMID: 16952835 DOI: 10.1263/jbb.102.41]

12 Török E, Vogel C, Lütgehetmann M, Ma PX, Dandri M, Petersen J, Burda MR, Siebert K, Düllmann J, Rogiers X, Pollok JM. Morphological and functional analysis of rat hepatocyte spheroids generated on poly(L-lactic acid) polymer in a pulsatile flow bioreactor. Tissue Eng 2006; 12: 1881-1890 [PMID: 16889518 DOI: 10.1089/ten.2006.12.1881]

13 Kinasiewicz A, Gautier A, Lewiska D, Smietanka A, Legallais C, Weryński A. Three-dimensional growth of human hepatoma C3A cells within alginate beads for fluidized bioartificial liver. Int J Artif Organs 2008; 31: 340-347 [PMID: 18432591]

14 Murtas S, Capuani G, Dentini M, Manetti C, Masci G, Massimi M, Miccheli A, Crescenzi V. Alginate beads as immobilization matrix for hepatocytes perfused in a bioreactor: a physico-chemical characterization. J Biomater Sci Polym Ed 2005; 16: 829-846 [PMID: 16128291]

15 Gerlach JC, Encke J, Hole O, Müller C, Ryan CJ, Neuhaus P. Bioreactor for a larger scale hepatocyte in vitro perfusion. Transplantation 1994; 58: 984-988 [PMID: 7974737 DOI: 10.1097/00007890-199411150-00002]

16 Vournakis JN, Runstadler PW. Optimization of the microenvironment for mammalian cell culture in flexible collagen microspheres in a fluidized-bed bioreactor. Biotechnology 1991; 17: 305-326 [PMID: 2049545]

17 Gåserød O, Sannes A, Skjåk-Braek G. Microcapsules of alginate-chitosan. II. A study of capsule stability and permeability. Biomaterials 1999; 20: 773-783 [PMID: 10353660 DOI: 10.1016/S0142-9612(98)00230-0]

18 Coward SM, Legallais C, David B, Thomas M, Foo Y, Mavri-Damelin D, Hodgson HJ, Selden C. Alginate-encapsulated HepG2 cells in a fluidized bed bioreactor maintain function in human liver failure plasma. Artif Organs 2009; 33: 1117-1126 [PMID: 20078562 DOI: 10.1111/j.1525-1594.2009.00821.x]

19 Nagaki M, Naito T, Ohnishi H, Akaike T, Muto Y, Moriwaki H. Effects of plasma from patients with fulminant hepatic failure on function of primary rat hepatocytes in three-dimensional culture. Liver Int 2005; 25: 1010-1017 [PMID: 16162161 DOI: 10.1111/j.1478-3231.2005.01127.x]

20 Chen Z, Ding Y, Li G. Configuration of a new bioartificial liver support system and in vitro evaluation of its functions. Ann Clin Lab Sci 2005; 35: 7-14 [PMID: 15830704]

21 Pan X, Li J, Du W, Yu X, Zhu C, Yu C, Cao H, Zhang Y, Chen Y, Li L. Establishment and characterization of immortalized human hepatocyte cell line for applications in bioartificial livers. Biotechnol Lett 2012; 34: 2183-2190 [PMID: 22930002 DOI: 10.1007/s10529-012-1025-1]]

22 Yu CB, Lv GL, Pan XP, Chen YS, Cao HC, Zhang YM, Du WB, Yang SG, Li LJ. In vitro large-scale cultivation and evaluation of microencapsulated immortalized human hepatocytes (HepLL) in roller bottles. Int J Artif Organs 2009; 32: 272-281 [PMID: 19569036]

23 Watanabe FD, Mullon CJ, Hewitt WR, Arkadopoulos N, Kahaku E, Eguchi S, Khalili T, Arnaout W, Shackleton CR, Rozga J, Solomon B, Demetriou AA. Clinical experience with a bioartificial liver in the treatment of severe liver failure. A phase I clinical trial. Ann Surg 1997; 225: 484-91; discussion 491-4 [PMID: 9193176 DOI: 10.1097/00000658-199705000-00005]

24 Xu X, Liu X, Ling Q, Wei Q, Liu Z, Xu X, Zhou L, Zhang M, Wu J, Huang J, Sheng J, Zheng S, Li L. Artificial liver support system combined with liver transplantation in the treatment of patients with acute-on-chronic liver failure. PLoS One 2013; 8: e58738 [PMID: 23516546 DOI: 10.1371/journal.pone]

25 Terblanche J, Hickman R. Animal models of fulminant hepatic failure. Dig Dis Sci 1991; 36: 770-774 [PMID: 2032519 DOI: 10.1007/BF01311235]

26 Donato MT, Castell JV, Gómez-Lechón MJ. Characterization of drug metabolizing activities in pig hepatocytes for use in bioartificial liver devices: comparison with other hepatic cellular models. J Hepatol 1999; 31: 542-549 [PMID: 10488716 DOI: 10.1016/S0168-8278(99)80049-X]

27 Naka S, Takeshita K, Yamamoto T, Tani T, Kodama M. Bioartificial liver support system using porcine hepatocytes entrapped in a three-dimensional hollow fiber module with collagen gel: An evaluation in the swine acute liver failure model. Artif Organs 1999; 23: 822-828 [PMID: 10491029]

P-Reviewer: Liu ZH        S-Editor: Wen LL             L-Editor:                  E-Editor:

Figure 1 Different components are labeled for reference. 1: Blood inflow; 2: Blood outflow; 3: Microcapsules accessing port; 4: Upper valve; 6: Lower valve; 5: Blood sample port; 7 and 8: Cell sieve; 9: Microcapsulated hepatocytes; 10: Choanoid container; 11: Cellular filter; 12: Buffer zone.

Figure 2 Fluidized bed bioreactor artificial liver. General setup includes the bioreactor hosting alginate/chitosan (AC) beads in the continuous fluidized bed motion.

Figure 3 Changes in alanine aminotransferase in encapsulated hepatocytes in medium experiment (n = 5). Levels are given as U/L (mean ± SD), (crosshatched bar) encapsulated in alginate/chitosan (AC) microcapsules and in static conditions; (gray bar) encapsulated in AC microcapsules and placed in the choanoid-fluidized bed bioreactor (CFBB). Student’s t test (aP < 0.05; bP < 0.01). NS: Not significant.

Figure 4 Secretion of albumin from encapsulated hepatocytes in medium experiment (n = 5). The levels are given as (g/L (mean ± SD), (crosshatched bar) encapsulated in alginate/chitosan (AC) microcapsules and in static conditions; (gray bar) encapsulated in AC microcapsules and placed in the choanoid-fluidized bed bioreactor (CFBB). Student’s t test (aP < 0.05; bP < 0.01). NS: Not significant.

Figure 5 Changes in alanine aminotransferase in encapsulated hepatocytes in exchanged plasma experiment (n = 5). The levels are given as U/L (mean ± SD), (crosshatched bar) encapsulated in alginate/chitosan (AC) microcapsules and in static conditions; (gray bar) encapsulated in AC microcapsules and placed in the choanoid-fluidized bed bioreactor (CFBB). Student’s t test (aP < 0.05; bP < 0.01). NS: Not significant.

Figure 6 Changes in TBil in encapsulated hepatocytes in exchanged plasma experiment (n = 5). The levels are given as (mol/L (mean ± SD), (crosshatched bar) encapsulated in alginate/chitosan (AC) microcapsules and in static conditions; (gray bar) encapsulated in AC microcapsules and placed in the choanoid-fluidized bed bioreactor (CFBB). Student’s t test. NS: Not significant.

Figure 7 Secretion of albumin from encapsulated hepatocytes in exchanged plasma experiment (n = 5). The levels are given as g/L (mean ± SD), (crosshatched bar) encapsulated in alginate/chitosan (AC) microcapsules and in static conditions; (gray bar) encapsulated in AC microcapsules and placed in the choanoid-fluidized bed bioreactor (CFBB). Student’s t test. NS: Not significant.

Figure 8 Transmission electron microscopy of alginate/chitosan-encapsulated cells in plasma before experiment (× 12000). A: Low-power view of a single spheroid with an alginate bead shows cohesive colonies of cuboidal cells; B: High-power view showing cytoplasmic organelles, and rough endoplasmic reticulum (RER), glycogen granules, and mitochondria; C: Extensive microvilli, bile canalicular formation, junctional complexes and desmosomes; D: Tight junction.

Figure 9 Transmission electron microscopy of alginate/chitosan-encapsulated cells in choanoid-fluidized bed bioreactor after 6 h plasma fluidization (× 12000). A, B, C: High-power view showing cytoplasmic organelles, and rough endoplasmic reticulum (RER), glycogen granules, and mitochondria; D: Small amount of vacuolization.

Figure 10 Transmission electron microscopy of alginate/chitosan-encapsulated cells in choanoid-fluidized bed bioreactor after 6 h static culture (× 12000). A: High-power view showing lots of organelles, mitochondria; B: High –power view showing some microvilli and tight junctions; C: A few nuclei showed shrinkage and some cells had vacuolar degeneration.